## Slide 1: Crushing Tools Management
Technical Development Program for PPE, 2015-2016

## Slide 2
2
Introduction to Wear Management
Wear Management - Crushing

## Slide 3
3
Why Wear Management?
Holcim prepares around 170 mio t/a of raw materials
  Crusher and raw mill work as a team to transform rock size product into meal for the clinker production process

## Slide 4
4
Both machines consume electrical energy and wear parts
  Wear at the crusher results in coarser feed size for the raw mill and lowers its efficiency
Wear & Electrical Energy Consumption
16kWh/t – 25 kWh/t
1.7 kWh/t – 3.0 kWh/t

## Slide 5
5
Adequate selection of wear parts combined with a good wear parts management strategy of the crusher could
  Decrease the specific wear rate at the crusher and associated maintenance costs
  Increase the energy efficiency of the raw mill by around 5% or 1 kWh/t of raw material
Potential Savings Through System Approach

## Slide 6
6
To optimise the whole size reduction chain you have to include mining operations!
  Blasting is the cheapest form of size reduction
  Finer blast saves money on loading, hauling & crushing
  Fragmentation is dependent of rock characteristics / geology
Further Influence: Raw Material Extraction

## Slide 7
7
Crusher Wear Parts
Wear Management - Crushing

## Slide 8
8
Impact & hammer crushers are the most commonly used machines
Holcim spends around 20 mio CHF/a for crusher wear parts
Significance of Crusher Wear Parts

## Slide 9
9
Wear Rates can be Expressed as NET or GROSS
Gross wear =
Initial weight
Production
What we pay
(GW)
Net wear =
Weight loss
Production
Indicates the material abrasiveness
(NW)

## Slide 10
10
6 month lifetime of manganese steel blow bars of an impact crusher correspond to around 10 g/t gross wear rate
Correlation between Lifetime & Wear Rate

## Slide 11
11
With wear parts being the leading cost factor, the importance of proper material selection becomes evident
Direct Cost of Wear

## Slide 12
12
Impact Crusher
Wear Management - Crushing

## Slide 13
13
Typical material of blow bars: Manganese steel
Impact Crusher

## Slide 14
14
3D carbide on manganese steel base
    Potential risk of inserts to break out from soft base
Ceramic inserts on martensitic steel base
New Blow Bars Technology
 Increase of lifetime and product size control for the raw mill

## Slide 15
15
Lifetime Factors for Blow Bars
Manganese steel
Martensitic steel
Ceramic Inserts on martensitic steel
3D-Carbide on manganese steel base
Manganese Steel resurfaced
Lifetime factor
1.0
--
1.30 – 1.8
2.0 – 3.0
~2.0 (2)
Primary
Secondary & Tertiary
1.0
--
1.5 – 2.0
2.5 – 4.0
(3)
High Chrome cast
Not Applicable
1.5 – 2.0 (1)
(1) Consistent performance over lifetime (reduced deformation)
(2) Results from initial tests
(3) No information available

## Slide 16
16
The blow bar design could be modified from manufacturing in order to adapt to the wear profile over the lifetime
  Allow for better product size control
  Increased utilisation of the blow bar weight (reduced gross wear rate)
Lifetime Influence through Blow Bar Design Modifications

## Slide 17
17
Grinding path with wear resistant plates
Breaker plates
Breaker Plates and Grinding Path for Product Size Control

## Slide 18
18
Hammer Crusher
Wear Management - Crushing

## Slide 19
19
Typical material of hammers: Manganese steel
Hammer Crusher

## Slide 20
20
Bimetal
  Head: Wear resistant cast (high chrome)
  Handle: Resilient steel
Martensitic steel (differential heat treatment)
  Head aimed at high wear resistance
  Handle aimed at high resilience
First Generation Hammer Improvements

## Slide 21
21
3D carbide on manganese steel base
Ceramic inserts on martensitic steel base
Latest Hammer Technologies
 Flexible design to adapt wear resistance of the hammer to the actual wear profile and thus achieve increased lifetime

## Slide 22
22
Lifetime Factors for Hammers
Manganese steel
Martensitic Steel diff. heat treatment
Ceramic Inserts on martensitic steel
3D-Carbide on manganese steel base
Manganese Steel resurfaced
Lifetime factor
1.0
1.1- 1.4
1.3 – 2.3
2.0 – 4.0
2 – 6 (1)
Primary
Secondary & Tertiary
1.0
(2)
1.5 – 2.0
2.0 – 4.0
(2)
Bimetal (High chrome cast head)
1.8 – 2.0
1.8 – 2.0 (1)
(1) More detailed investigations required for range clarification
(2) No information available

## Slide 23
23
Anvil and Grates for Product Size Control
Anvils and crusher basket bars with 3D-Carbide
Resurfaced crusher basket edges

## Slide 24
24
Lifetime and Throughput Influence by Hammer Design
Original
Modified

## Slide 25
25
Other Crusher Types
Wear Management - Crushing

## Slide 26
26
Double Roller Crusher
Replaceable plates
Replaceable inserts
Regular regeneration of teething through weld deposited material
Used solution is much dependent on crusher make

## Slide 27
27
Mineral Sizer
Exchangeable wear caps
Primary
Secondary
Hazemag (plates)
Bedeschi (rings)

## Slide 28
28
Weld deposited wear resistant material to protect most exposed zones
Rotor Wear Protection for IC / HC / DRC

## Slide 29
29
Typical solution: Manganese steel plates combined with different plate geometries
    Regeneration of plates at the lower part through weld deposited material is possible
Jaw Crusher

## Slide 30
30
Mantle and concave liners are generally glued to shaft / shell
Refurbishing through welding is possible, but needs to consider impact on glue
  On site or in workshop
Gyratory Crusher
Main shaft mantle
Concave liner

## Slide 31
31
Cones can be rewelded or even equipped with 3D-Carbide
Generally they are replaced due to size and cost
Cone Crushers

## Slide 32
32
Crusher and raw mill have to be optimised as one system
Wear at the crusher has an influence on the raw mill
  Decreased throughput
  Increased electrical energy consumption
  Decreased reliability / stability
Most crushers still use locally manufactured manganese steel parts
Latest technology crushing tools can lead to substantial savings in
  Wear parts cost
  Electrical energy for raw grinding
  Maintenance work
Summary