## Slide 1: Materials Uniformity and Quality Control
PPE Course

## Slide 2
2
Understand quality indicators from legacy Holcim and Lafarge
Be able to use quality data for root cause analysis
Be aware of cost impacts of inadequate uniformity
Know effective quality control measures
Objectives

## Slide 3: Agenda
Introduction
5
Quality and Uniformity Targets
10
Evaluation of uniformity
23
Cost Impact of Insufficient Uniformity
52
How to improve uniformity
67
Quality Control Aspects of Uniformity
75
Summary and Conclusions
85

## Slide 4: Introduction

## Slide 5
5
Accused in the context of:
kiln commissioning
low kiln availability
low kiln production rate
high refractory wear
limited AFR utilisation
clinker/cement
quality deficiencies
Importance of kiln feed uniformity
Chart: LS
There is a great potential to exploit!

## Slide 6
6
Cost effective processing of materials requires:
  Appropriate targets for relevant material properties
  High uniformity of material properties
Deviations from targets and excessive variations lead to higher production costs and final product deficiencies
Targets and Uniformity: Objectives
 Non-Quality Costs

## Slide 7
7
Relevant material properties
Process | Material | Relevant materials properties for process and quality
Quarrying | Raw components | Major elements: SiO2, Al2O3, Fe2O3, CaO Minor elements: alk., SO3, Cl, MgO, TOC Mineralogical composition: quartz Moisture
Storage/ Preblending | Components, blended components | Major elements: SiO2, Al2O3, Fe2O3, CaO Minor elements: alkalis, SO3, Cl, MgO Mineralogical composition: quartz Granulometry
Raw meal grinding | Raw meal | Major elements: LS, SR, AR (alkali) Minor elements: alk., SO3, Cl, MgO, TOC Mineralogical composition: quartz Fineness: R90mm
red: only place to control gray: limited or no direct control possibility

## Slide 8
8
Relevant material properties
Process | Material | Relevant materials properties for process and quality
Clinker burning | Kiln feed | Major elements: LS, SR, AR (alk.) Minor elements: alk., SO3, Cl, MgO, TOC Mineralogical composition: quartz Fineness: R90mm
 | Fuels, AFR | Fineness Calorific value S, Cl, others
 | Clinker | Free lime Major elements: LS, SR, AR (alk.) Clinker phases: C3S, C2S, C3A, C4AF
Cement grinding | Cement/ Mortar | Fineness: Blaine, R45mm, SO3 Strength

## Slide 9: Quality and Uniformity Targets

## Slide 10
10
Legacy Holcim Performance Radar: Product uniformity was part of it

## Slide 11
11
Six (potential) quality indicators for performance monitoring
Index | Indicator | 
Product Quality Index | 1 | Measurement of customer satisfaction
 | 2 | Product performance benchmarking against competitors
 | 3 | Clinker factor (new)
 | 4 | Product compliance to internal product specifications
 | 5 & 6 | Manufacturing quality targets and KPIs
 | 7 | Lab methods mastery (new)
Marketing
Manufacturing
Responsibility:

## Slide 12
12
Specific targets and the respective score for the Product Quality Index

## Slide 13: Product Quality Index development 2009 - 2014
New calculation in 2014
Chart: PQI (total rating) 2009 - 2014
| 2009 | 2010 | 2011 | 2012 | 2013 | 2014
low potential | 30.4 | 45.3 | 60.4 | 63.8 | 67.8 | 49.4
moderate potential | 64.1 | 50.5 | 33.3 | 36.1 | 32.2 | 43.3
high potential | 5.4 | 4.2 | 6.3 | 0 | 0 | 7.2

## Slide 14
14
Manufacturing quality targets and KPIs: Product uniformity
Legacies | Parameters | Targets
Holcim |  | 
 | 2-days strength CoV | ≤ 6%
 | 3-days strength CoV | ≤ 4%
 | 28-days strength CoV (old) | ≤ 3%
Lafarge |  | 
 | 28-days standard deviation | Classes A-E (example EN) < 1.6 1.6 – 2.0 2.0 – 2.5 2.5 – 3.0 > 3.0

## Slide 15
15
Legacy Holcim:
  The indicator measures the percentage of clinker volume where all clinker specifications are fulfilled
  Specifications have to be fulfilled on two levels: First level (mandatory)
Comparison with legacy Lafarge:
  Lime saturation range ± 2.5 corresponds to CUI variance class C
  Free lime range of 1.5 corresponds to FLUI class C
Compliance to Clinker Specifications
Free Lime |  |  | Lime saturation |  | 
 | Acceptance range |  |  | Acceptance range | 
 | Min. | Max. |  | Min. | Max.
Tfree lime | Tfree lime -0.5 | Tfree lime +1.0 | Tlimesaturation | Tlimesaturation – 2.5 | Tlimesaturation +2.5

## Slide 16: Legacy Lafarge kiln feed and clinker uniformity indicators
By definition, calculated based on 1 sample per day at specific time: For example, 8am clinker sample, 6am kiln feed sample
Kiln feed uniformity calculated vs Target, others vs Average

## Slide 17
17
Excellent … and poor uniformity
Plant B
Conformity 34 % (LS and CaOf)
Plant A
Conformity 91 % (LS and CaOf)
LS
CaOf
2-hourly testing frequency, 1 month period

## Slide 18
18
Legacy Holcim uniformity targets: Kiln feed (and clinker)
* For plants with pre-blending systems
The ultimate goal is to achieve a high chemical uniformity of clinker
*

## Slide 19
19
  Second level (plant specific selection, not mandatory)
    Specifications for C3A, Na2O eq., SO3, F and for other plant relevant minor elements (e.g. MgO, P2O5, etc.)
    They have to be specified in case they are relevant to meet the Internal Product Specifications and related National Cement Standards (e.g. low alkali cements, sulfate resistant cements, cements made with mineralized clinker).
    Following one example:
Compliance to Clinker Specifications (cont.)
C3A |  |  | Na2O-equivalent |  | 
 | Acceptance range |  |  | Acceptance range | 
 | Min. | Max. |  | Min. | Max.
7.0 | 5.0 | 8.0 | 0.50 | n.d. | 0.6

## Slide 20
20
Additional criteria for clinker/raw meal uniformity
Clinker | Daily (hourly samples) | Monthly (daily averages)
CaO f Range Min.- Max. (%) |  1.5 | ND
SO3 C.o.V. |  10%* | ND
K2O C.o.V |  10%* | ND
Raw Meal | Daily (hourly samples) | Monthly (daily averages)
Fineness R90 C.oV.* |  5% | ND
* MPR target for excellence

## Slide 21
21
Uniformity Indicators – Benchmarks
2 3 4 5 6 7 8 9 10 11 12 13
Plant No.
Plant No. | Std LS Kiln feed | Blending factor
1 | 0.61 | 2.2
2 | 0.62 | 1.8
3 | 0.79 | 1.2
4 | 0.89 | 2.2
5 | 0.89 | 2.2
6 | 1.01 | 1.5
7 | 1.07 | 1.6
8 | 1.19 | 3.0
9 | 1.26 | 2.5
10 | 1.28 | 3.5
11 | 1.34 | 0.9
12 | 1.45 | 3.8
13 | 1.69 | 0.5

## Slide 22: Evaluation of uniformity

## Slide 23
23
Evaluation of short term and long term variability over one month
 |  |  |  |  | 01.08.2015 | 02.08.2015 | 03.08.2015 | 04.08.2015 | 05.08.2015 | 06.08.2015
 | CoV | Average | Stdev |  | Date | Date | Date | Date | Date | Date
 |  |  |  |  | 42217 | 42218 | 42219 | 42220 | 42221 | 42222
Long term | 1.74% | 100.94 | 1.76 | x LS | 100.31 | 100.11 | 100.03 | 99.79 | 99.94 | 101.11
Short term |  | 3.55 |  | s LS | 1.34 | 1.26 | 5.23 | 4.69 | 2.56 | 1.24
 |  |  |  | cov LS | 1.33% | 1.26% | 5.23% | 4.70% | 2.56% | 1.23%
 |  |  |  | min LS | 98.01 | 98.18 | 89.14 | 92.39 | 95.69 | 99.41
 |  |  |  | max LS | 102.18 | 102.25 | 108.83 | 107.73 | 104.89 | 103.34
 |  |  |  | n LS | 15 | 9 | 11 | 8 | 13 | 11
Long term | 2.99% | 2.45 | 0.07 | x SR | 2.49 | 2.49 | 2.49 | 2.43 | 2.50 | 2.46
Short term |  | 0.06 |  | s SR | 0.04 | 0.04 | 0.11 | 0.12 | 0.04 | 0.03
 |  |  |  | cov SR | 1.62% | 1.45% | 4.45% | 4.83% | 1.69% | 1.31%
 |  |  |  | min SR | 2.41 | 2.44 | 2.32 | 2.26 | 2.41 | 2.39
 |  |  |  | max SR | 2.56 | 2.55 | 2.66 | 2.55 | 2.56 | 2.50
 |  |  |  | n SR | 15 | 9 | 11 | 8 | 13 | 11
Long term | 1.88% | 1.47 | 0.03 | x AR | 1.45 | 1.47 | 1.47 | 1.50 | 1.43 | 1.45
Short term |  | 0.06 |  | s AR | 0.06 | 0.07 | 0.04 | 0.06 | 0.04 | 0.01
 |  |  |  | cov AR | 3.98% | 4.71% | 3.04% | 4.28% | 2.59% | 0.85%
 |  |  |  | min AR | 1.38 | 1.36 | 1.39 | 1.43 | 1.35 | 1.43
 |  |  |  | max AR | 1.58 | 1.60 | 1.53 | 1.60 | 1.49 | 1.47
 |  |  |  | n AR | 15 | 9 | 11 | 8 | 13 | 11

## Slide 24: Evaluation of short term and long term variability
red: LS standard deviation
blue: average LS
s LS
x LS

## Slide 25
25
Short term variability:
  Average of the daily standard deviation (s) over one month (e.g. on hourly or two-hourly samples)
  Particularly relevant for equipment performance
Long-tem variability:
  Standard deviation of the daily average values (s) over one month
  Particularly relevant regarding product quality
Short term and long term variability calculated over one month

## Slide 26
26
Short term variation (standard deviation) should be only calculated with more than 4 (better 6) samples.
Long term variation is dependent on the number of samples used to calculate the daily average
Change of targets will have effect on long term variation
If there is a clear change of targets, the time periods could be split
Long term and short term variation do not necessarily need to correlate
Evaluation of uniformity: Considerations

## Slide 27
27
Long term uniformity: Effect of taking averages
All these averages come from the sample population!

## Slide 28
28
Detailed quality data analysis serves to find root causes for excessive variability. This, in turn, is the basis to define measures for improvement.
Average values and standard deviation can point towards existing variability problems, but are generally not sufficient to derive causes.
Effective tools are graphical representations, supported and complemented by statistical tools.
Quality Data Analysis

## Slide 29
29
Plant subject to heavy coating, ball and ring formation, as well as instable coating, attributed to chemical variations in kiln feed
Plant also wants to rationalize laboratory work
Variability Assessment: Plant Example

## Slide 30
30
Variability Assessment of LS: Plant Example
individual data points
LS of hourly samples in raw meal
std = 1.9
averages
daily averages
std = 0.6
standard deviation
standard deviations over 1 day
std = 1.3 (average)

## Slide 31
31
Variability Assessment of SR: Plant Example
individual data points
SR of hourly samples in raw meal
std = 0.30
averages
daily averages
std = 0.29
standard deviation
standard deviations over 1 day
std = 0.08 (average)

## Slide 32
32
Variability Assessment: Plant Example

## Slide 33
33
Variability Assessment: Plant Example

## Slide 34
34
Assessment
  Short term variability is good; LS of raw meal can be well controlled with preblended limestone and preblended clay
  Temporary disturbances due to stockpile endcones
  Step changes in SR due to different compositions of successive preblending stockpiles
Recommendation
  Improve deposit knowledge to better manage SR; PGNAA possible, but no benefit for endcones and rationalization
  Automate raw meal control; option to extend automation to other areas: helps for endcones, permits rationalization
Realized: Local on-line raw meal control (FLS On-Stream) (not optimal for rationalization)
Variability Assessment: Plant Example

## Slide 35
35
Time plot provides insight into variability pattern
out of control
stable
Trend

## Slide 36
36
Influences of fuel mix on clinker uniformity

## Slide 37
37
Classification: Cycles and trends
Normal behavior
Trends
Cycles

## Slide 38
38
Classification: Cycles and trends
median
runs
Runs
Expected number of runs = (n + 2) / 2 (process under control)
Relevance for raw meal control:
  Too long periods above or below a given target value (e.g. lime saturation) can no longer be blended out in the homogenization silo. Sufficiently frequent cross-overs of target line is desirable.

## Slide 39
39
Classification: Cycles and trends
Mean square successive difference

## Slide 40
40
Classification: Cycles and trends
 | MSSD-Stdev | Actual runs
Normal behavior |  Stdev |  expected runs
Trends | < Stdev | << expected runs
Cycles | > Stdev | >> expected runs
Indicators

## Slide 41
41
Situation
  New production line
  On-line raw meal control with local system (Polysius AOT), permitting XRF-analysis and feeder adjustments in intervals as short as 10 minutes
  Components: Limestone, clay, fly ash, mill scale
  Guarantee tests for achieving blending performance Procedure: every hour, the average LS over the past 2 hours is determined. 95 % of these values have to be within target LS ± 2 % (same for SR and AR)
Process Behavior: Plant Example

## Slide 42
42
Process Behavior: Plant Example
Std = 7.2
MSSD-std = 2.3 (2.3 << 7.2
Runs = 7 (7 << 27)
Process subject to trends

## Slide 43
43
Process Behavior: Plant Example
set-point (%) clay
actual (%) limest.
actual (%) clay
set-point (%) limest.
% clay

## Slide 44
44
Assessment
  Swing (trend) is caused by slow response of feeders
  Complex system of overriding loops and feeder links are preventing the immediate application of the requested feeder set-points
  Direct feed of clay from Bedeschi stockpile, without intermediate feed bin (stickiness). Clay respond particularly slow.
Solutions
  Elimination of overriding loops and tuning of blending program by plant process engineer and supplier. Significant improvements made.
  Improvements of clay feed difficult.
Process Behavior: Plant Example

## Slide 45
45
Clay feed system

## Slide 46
46
Statistically, points should be in between
and
     is mean  is standard deviation
Idea is based on probability theory
  Only 0.3%, out of 3 control limit (normal distribution)
  Rare event  interpret as out of control (something wrong)
Statistical process control: Basics
-3σ
μ
+3σ
99.7%
Points are unlikely to be out of ( ± 3) range … If we can assume normal distribution

## Slide 47
47
Control limits:
Estimation of parameters:
  Expected mean
  Standard deviation: Either global variability
  or local variability (using the range of two values)
X-Chart: Control limits for individual values

## Slide 48
48
Is this process under control?

## Slide 49
49
Example: X-chart

## Slide 50
50
Process capability: Factors
Sample Size n
Factors for
Factors for Standard Deviation or Sigma
d2
Sample Size n
Average
A2
Range
D3
D4
2
1.880
.0
3.268
1.128
2
3
1.023
.0
2.574
1.693
3
4
.729
.0
2.282
2.059
4
5
.577
.0
2.114
2.326
5
6
.483
.0
2.004
2.534
6
7
.419
.076
1.924
2.704
7
8
.373
.136
1.864
2.847
8
9
.337
.184
1.816
2.970
9
10
.308
.223
1.777
3.078
10
11
.285
.256
1.744
3.173
11
12
.266
.284
1.717
3.258
12
13
.249
.308
1.692
3.336
13
14
.235
.329
1.671
3.407
14
15
.223
.348
1.652
3.472
15

## Slide 51: Cost Impact of Insufficient Uniformity

## Slide 52
52
Increased production volume
Lower specific thermal energy consumption
Reduction of off-spec clinker volume
Lower specific consumption of refractory materials
Improved clinker reactivity
Reduced specific energy consumption for cement grinding
Potential benefits resulting from improved kiln feed uniformity

## Slide 53
53
Polysius: 1-2% more energy efficient clinker and cement production:
  1 mio t of clinker with 3.5 GJ/t, 3 EUR/GJ for thermal energy: 1.5 % energy savings translates into yearly savings of 160’000 EUR
  1.5 mio t of cement with 100 kWh/t, 0.15 EUR/kWh for electrical energy: 1.5 % energy savings translates into yearly savings of 340’000 EUR
FLS: Reduction of specific heat consumption by 100 MJ/t of clinker by improvement of LS standard deviation of kiln feed by 1:
  1 mio t of clinker with 0.1 GJ/t reduction, 3 EUR/GJ for thermal energy: improved uniformity translates into yearly savings of 300’000 EUR
Estimation of financial benefits resulting from improved uniformity

## Slide 54
54
Example: Specific thermal energy consumption
Heat consumption
versus kiln feed quality
data from FLSmidth study:
a 1 % increase in LSF std dev = +25 kcal/kg
1 mio t of clinker with 0.1 GJ/t reduction, 3 EUR/GJ for thermal energy: Improved uniformity translates into yearly savings of 300’000 EUR

## Slide 55
55
Very poor correlations are observed. Heat consumption is affected by many other parameters.
However, positive correlation is indicated
Similar order of magnitude as in FLS study (100 kJ/t per 1 point s(LS))
Specific heat consumption and s(LS) for three (random) plants
Chart: EC Jul-Nov 2013
Chart: LN May-Nov 2013
Chart: CP Jul-Nov 2013

## Slide 56
56
Concept of Defining Minimum Requirement
Avg 2
S = 1.5
Avg 1
S = 2.5
Minimum
Quality
Requirement
a = 5 %
Non Quality
Costs
Quality Parameter

## Slide 57
57
Situation
  Plant with 4-stage preheater reports the experience that the specific heat consumption increases by 15 MJ/t clinker for an increase in lime saturation by one unit.
  Assuming a minimum requirement of 91 LS, the savings related to a decrease of standard deviation from 2.5 to 1 LS can be calculated.
  See also Report MA 94/3198/E
Non-Quality Cost: Impact Kiln Feed Variability

## Slide 58
58
Non-Quality Costs Related to Product Variability
Minimum Requirement
91.5 % LS
Reduction in Variability (STD)
2.5 LS to 1 LS
Specific Savings
15 MJ /t. LS
Absolute Savings
46 MJ /t
Annual Clinker Production
0.8 Mio t
Energy Costs per Unit
2.5 USD /GJ
Savings per Year
92'000 USD
Clinker Burning

## Slide 59
59
Non-Quality Cost: Impact Cement Variability
10.11.2010
actual values
Average 43.8 MPa
Std Dev 2.3 MPa
CoV 5.2 %
95% = +/- 2 s
% Observations
0
2
4
6
8
10
12
14
16
18
36.0
37.0
38.0
39.0
40.0
41.0
42.0
43.0
44.0
45.0
46.0
47.0
48.0
49.0
50.0
51.0
52.0
28 d strength [MPa]
% Observations
Holcim target
CoV 3.0 %
Std Dev 1.3 MPa
95% = +/- 2 s
– 2 MPa
Average 41.8 MPa
28 d strength [MPa]
OPC Type I/II

## Slide 60
60
Plant produces Type I/II and Type III from same clinker, cements differ in fineness only. Relevant data from ATR:
Non-Quality Cost: Impact Cement Variability
 | Type I/II | Type III | 
Fineness Blaine [cm2/g] | 3825 | 5120 | 1295
Specific energy cons. [kWh/t] | 48.1 | 70.9 | 22.8
28 d strength [MPa] | 42.5 | 50.4 | 7.9
 164 Blaine/MPa
 1.76 kWh/t.100 Blaine

## Slide 61
61
Impacts of Cement Uniformity
2 MPa  300 Blaine
Type III
Type I
Example from MPR:
Estimation: 300 Blaine » 5.2 kWh/t

## Slide 62
62
Better uniformity allows for more flexibility to react to market needs
28 Days Strength in Mpa
65
62.5
Conformity Range for
60
Average Strength
55
Better Quality / Cost Ratio
Flexibility in Product Diversification
50
Better Competitiveness
45
42.5
40
1
2
3
4
5
6
7
Standard Deviation in Mpa

## Slide 63
63
Costs related to outside storage of clinker
Costs of additional handling
Pre-hydration of clinker: Loss of reactivity, harder to grind.
 Increase of specific grinding energy, higher clinker factor

## Slide 64
64
Situation
  Plant A stocks 50’000 t clinker outside during the rainy season because of low cement demand. Moisture contents increases to 5 %. Clinker needs to be crushed.
  Plant B is located in a dry climate. Outdoor clinker is not hydrated; nevertheless, costs arise due to double handling and need to grind to higher Blaine.
    (example from Report MA 94/3190/E)
Costs related to outside storage of clinker: Example

## Slide 65
65
Costs Associated with Outdoor Stored Clinker

## Slide 66: How to improve uniformity

## Slide 67
67
Clinker and Cement uniformity is the result of all steps of manufacturing
RAW MILL /
HOMOGENIZATION
PREBLENDING
CLINKER
BURNING
QUARRY
CLINKER/ CEMENT
CEMENT
GRINDING

## Slide 68
68
Measures to Improve Uniformity
Process | Quality Control | Process
Quarrying |  | 
Storage/ Preblending |  | 
Raw meal grinding |  | 
Homogeni-zation |  | 

## Slide 69
69
Measures to Improve Uniformity
Process | Quality Control | Process
Quarrying | Blast drill hole analysis QuarryMaster | Selective quarrying
Storage/ Preblending | Bulk Material Analyzer (PGNAA) | Preblending beds Optimization end cones
Raw meal grinding | Frequent raw meal control On-line control by PGNAA ahead of mill On-site XRF- system Central lab automation | Upgrade feed systems Modify dust handling
Homogeni-zation | Frequent kiln feed control Autom. kiln feed control (central lab automation) | Kiln dust handling (compound vs direct operation) Maintenance of blending silos Silo operation

## Slide 70
70
Measures to Improve Uniformity
Process | Quality Control | Process
Fuel preparation |  | 
Clinker burning |  | 
Cement grinding |  | 

## Slide 71
71
Measures to Improve Uniformity
Process | Quality Control | Process
Fuel preparation | Frequent fineness control | Regular AF availability and dosage
Clinker burning | Frequent free lime control Autom. free lime control On-site free lime analyzer XRD in central lab Autom. clinker phase control (Rietvelt analysis) Hot meal control | Regular kiln feed and fuel feed rate Kiln Expert Control
Cement grinding | Frequent fineness control Autom. fineness control On-site fineness analyzer fineness in central lab Autom. chemical control central laboratory | Preblending of MIC Individual feed systems for each constituent Upgrade feed systems

## Slide 72
72
Uniformity is affected by incomplete filling of pre-blending piles

## Slide 73
73
Inadequate feed size causes feeder blockages

## Slide 74: Quality Control Aspects of Uniformity

## Slide 75
75
Increased product quality and reduced operational costs through improved uniformity
  High sampling frequency
  More sampling points
  Round-the-clock control
  High standard of sample preparation and analysis
  Measurement of relevant parameters at high frequency
    Ideally “real time” / At earliest opportunity
    Fast reaction (process control)
Automated QC systems need an appropriate control software
Liberation of personnel from routine work for more demanding tasks – Especially shift laboratory
Automation in quality control helps to improve uniformity

## Slide 76
76
Advantages
  Installed on mill feed belt
  <5 min control interval
Limitations
  All components have to be on mill feed belt
  Space requirement
Appropriate for
  Heterogeneous raw components
  Mill systems with long retention time
  Very large capacity mills
Examples: PGNA Analyzer on Raw Mill Feed
USD 350,000 approximately

## Slide 77
77
Typical setup for raw mix control
PLC
Fe
Al
Si
CCM
Operator console
Balance
Pre
Mix
PGNAA
Electronic
Enclosure
Raw Mill
Control
Software

## Slide 78
78
Example: Improved uniformity through PGNAA control

## Slide 79
79
Advantages
  Approx. 10 min control interval
  Optimum sample preparation
  Mechanically complex, but “high quality” design
Limitations
  Higher price
Application
  2 systems installed (HH, JO)
Experience
  High availability; well performing system
No longer marketed by Polysius
Examples: Polysius AOT Analyzer (XRF)
USD 300,000 approximately

## Slide 80
80
Laser granulometer systems are established solutions in the laboratory.
Online systems: Real-time information for process control (e.g transition between two products)
Online systems from Malvern (Insitec) and Sympatec (MYTOS).
Limited applications in Holcim (15 – 20 units installed).
Preferred technology by HGRS, though cost/ benefit often not evident. Multiple mill units render concept expensive.
Examples: Cement Fineness with Malvern/Insitec
Primary sampling
Secondary sampling
Analyzer
Material return

## Slide 81
81
Automated laboratories help to increase sampling and analysis frequency
Automated sampling and dispatch
Pneumatic sample transport
Automated sample reception and preparation
Integrated analytical equipment
Control Software

## Slide 82
82
Centralized Control Systems
X-ray room
(15-20 sqm)
Sample prep room
(30-40 sqm)
FLS RoboLab
QCX/RoboLab

## Slide 83
83
FLS RoboLab at St. Genevieve

## Slide 84: Summary and Conclusions

## Slide 85
85
High material uniformity is essential for high equipment performance. Deficiencies cause appreciable non-quality costs and can impair competitiveness.
Quality control and quality data do not only serve for on-going control, but also to analyze process performance.
It is the task of the Process Engineer, in cooperation with the quality responsible, to investigate improvement potentials and to develop solutions. Measures both in quality control and process may be required.
Powerful automated quality control technologies are available; their cost-effectiveness, however, needs to be evaluated carefully.
Summary and Conclusions