## Slide 1: Practical Aspects of Sampling
PPE Course

## Slide 2: Objectives
Understand the difference between systematic and random errors
Be aware of the three golden rules of sampling
Know the sampling points along the process
Be able to provide recommendations for proper sampling points and equipment

## Slide 3: Agenda
Introduction
4
Sampling points along the process
9
Sampling of coarse bulk material
12
Sampling of fine material (powder)
24
Summary
39
Annex
41

## Slide 4: Introduction

## Slide 5
5
Sample
Preparation
Analysis
Result
Effect
Action
Decision
Interpretation
s1
s2
s3
Sampling forms the basis for process control
Typically: s1 >> s2 > s3

## Slide 6
6
There are two basic error types with sampling
Systematic Errors
Random Errors
Biased samples
Deviation to the real value can not be calculated
Unbiased samples
Deviation to the real value can be calculated with statistics
Not Representative
Not all particles have the same chance to enter the sample.
Representative!
Random errors:
- Error of analysis: sA2
- Fundamental error: sST2
- Error of variability: sS2
[ Systematic errors can not be quantified. They can be detected by cross-checks with alternative procedures.]

## Slide 7
7
Illustration: Compositional heterogeneity
Thin sections of marly-type limestone (same magnification)
Smaller s2(c)
Larger s2(c)
The composition variance s2(c) is sometimes also called ‘small scale heterogeneity’, denoted as I [kg%2].

## Slide 8
8
The three golden rules of sampling
  Always sample on a falling stream
  Sample the whole cross-section of the stream
  Combine single samples into a composite sample (rule of thumb: 15 single samples into one composite)
Easy in theory – hard to achieve in practice.
How to obtain bias free samples
All particles in the stream must have the same probability to enter the sample.

## Slide 9: Sampling points along the process

## Slide 10
10
2
3
5
4b
9
8
7
6
11
10
1
4a
Sampling points along the process

## Slide 11
11
We’ll group the materials into two classes
4b
5
6
7
10
11
Raw meal
Kiln feed
Hot meal
Fine coal
Cement, ex mill
Cement, dispatch
Powdered Materials
1
2
3
8
9
Drill hole chips
Pre Mix (stockpile)
Correctives
Raw mix
Clinker
Additives
4a
Coarse Materials

## Slide 12: Sampling of coarse bulk material

## Slide 13
Premix after crusher
Objective
Material
Mode
Type
Frequency
Location
Quantity
Equipment
Transport
Manual
Chemical composition of pre-mix Adjusting materials fed to the crusher Control stockpile composition
Semi-automatic, automatic
Composite and/or spot
e.g. once per hour
Conveyor belt after crusher
100 kg and more
Hammer, spoon sampler or Sampling tower
Mix of: limestone, marl, clay
PGNA is state of the art technique for premix control

## Slide 14
14
PGNAA*, standard solution for in-line analysis of bulk material on belt conveyor
* Prompt Gamma Neutron Activation Analyzer

## Slide 15
15
Coarse bulk material – sample quantity vs. top particle size
kg
e.g. crushed limestone
e.g. Iron ore
ca.
70kg
ca.
1kg

## Slide 16
16
Manual sampling from a running conveyor belt
  Is a safety hazard
  Does not provide a meaningful sample for process control
Avoid sampling from running conveyor belt

## Slide 17
17
Design: Distance between side plates of hammer > 3 * top size of material
Rotating velocity (bouncing of coarse particles)
Biased if height/shape not properly adjusted
Rotating scoop (hammer) sampler – not suitable for routine control

## Slide 18
18
Use of sampler cutter. In principle correct, if all material is removed. Sometimes applied for PGNAA calibration.
Stopped belt sampling – not suitable for routine control
Disadvantages: Production stop, not practical for > 20 samples (belt drive), not working at inclined belts.

## Slide 19
Clinker sampling
Objective
Material
Mode
Type
Frequency
Location
Quantity
Equipment
Transport
Manual or pneumatic (needs on-site sample preparation)
Ensure correct burning regime by measuring chemical composition and free lime
Manual/semi automated/automated
Spot sample / composite sample
~ once per hour (min every 4 hours)
Transfer points/transport after cooler, drilled cooler plate
2 – 5 kg / sample
Piston, scoop sampler
Clinker

## Slide 20
20
Safety issue
Representativity not given
Manual sampling – not recommended

## Slide 21
21
Clinker sampler (spoon sampler): Preferred solution
Installation: free falling material stream
Sampling point: material chute
Sampling type: spot sampling
Sample material: coarse, clinker
Particle size: max. 100 mm
Temperature: max. 250 °C
Sample quantity: app. 15 dm3/pass
Sample cycles: < 20 cycles / h
Sampler weight: up to 550 kg

## Slide 22
22
Clinker sampler with downstream sample preparation
Clinker transport
Spoon sampler
Vibration feeder
Crusher
Sample splitter
Fine grinding mill
Mixer
Dosing unit
Pneumatic tube
sending station
Collection cup
Automatic sieve
Measuring cup with leveling and balance

## Slide 23
23
Automated clinker sampling: Example

## Slide 24: Sampling of fine material (powder)

## Slide 25
Raw meal sampling
Objective
Material
Mode
Type
Frequency
Location
Quantity
Equipment
Transport
Manual, pneumatic tube system (preferred)
Chemical analysis for raw mix and feeder control
Sieve or PSD analysis for separator adjustment
semi automated/automated
Composite sample
Hourly or 2-hourly
After raw mill cyclone before homo silo. Bag-house dust added.
2 – 5 kg / sample
Screw sampler. (Air slide sampler: not optimal)
Raw meal, finish product

## Slide 26
Kiln feed sampling
Objective
Material
Mode
Type
Frequency
Location
Quantity
Equipment
Transport
Manual or pneumatic tube system
Monitoring of feed uniformity (chemistry and fineness)
semi automated/automated
Composite sample (option for spot)
Every 2-4h
Transfer behind homo silo to feed system, after last material added (e.g. kiln dust)
2 – 5 kg / sample
Screw sampler. (Air slide sampler: not optimal)
Kiln feed

## Slide 27
Cement (ex mill) sampling
Objective
Material
Mode
Type
Frequency
Location
Quantity
Equipment
Transport
Manual, pneumatic tube system (preferred)
Control of feed system and separator adjustment (chemistry and fineness) Monitor physical properties
semi automated/automated
Composite sample (spot sample)
Hourly or 2-hourly
Behind mill, transport to storage silo
2 – 5 kg / sample
Screw sampler. (Air slide sampler: not optimal)
Cement

## Slide 28
28
Recommended sampling system:
  Automated screw sampler including mixer, splitter and excess return. Sampler must allow programming of extraction sequences.
Pay attention to
  Appropriate position (across material flow)
  Distance to transfer points (e.g. dust return) and de-dusting systems
  Pressure situation (no draft through the sampling system)
  Drop height of sample (< 10 m)
  Protection and maintenance of sampler (avoid exposure moisture)
  Sampler accessibility
General remarks on sampling of powdered materials

## Slide 29
29
Screw sampler installation: Always across material flow

## Slide 30
30
Raw meal
Filter dust
Raw mill product
Comments on the sampling point:
  Incorrect direction of screw
  Too close to mixing point
Search for alternative lower in the chute

## Slide 31
31
Screw sampler: Standard solution for powders

## Slide 32
32
Automated screw sampler with mixer, splitter and sending station
Double screw sampler
Shut off valve
Mixer
Dosing unit
Material return
Pneumatic tube sending station

## Slide 33
33
Air slide sampler
Air slide samplers should only be installed if there is no room for screw samplers (consider transfer chute between two air slides).
Continuous or spot sample
Material: powdered, not sticky
Max particle size: 2 mm
Max. temperature: 120 °C
Sample quantity: up to 22 kg/h
Cycles: < 30/h

## Slide 34
34
Air slide sampler
Material flow
What is the correct position for an air slide sampler?

## Slide 35
Hot meal sampling
Objective
Material
Mode
Type
Frequency
Location
Quantity
Equipment
Transport
Manual / pneumatic tube system
Measure Cl, SO3, Alkalis and LOI to control the degree of calcination and as indicator for build-up formations
manual/automated
Spot sample
Once every 4 hours / on demand
Outlet bottom cyclone towards kiln inlet
Approx. 1 kg
scoop / piston sampler
Calcinated meal

## Slide 36
36
Hot meal sampling is potentially dangerous (raw meal flushes).
Direct contact with hot meal must be avoided.
Safe manual and automated sampler are available.
Hot meal sampling
FLS design
Lit: ZKG International, 2003, 56, 34

## Slide 37
37
Automated hot meal sampling
Example: SG (CH)
Water cooling
Costs: 70 k€

## Slide 38
38
Summary of recommended sampling devices according to the material type

## Slide 39: Summary

## Slide 40
40
Sampling of coarse bulk material for process control is not practicable with the available resources (time/manpower). If required for special tests, large sample masses (> 500 kg) and high preparation effort can be expected.
Every sampling procedure has errors. Representativeness of a sample needs to be evaluated with respect to the required accuracy.
Adequate sampling installations in cement plants need to be integrated during design of the plant. Good sampling installations need space.
Summary

## Slide 41: Annex

## Slide 42
42
Raw meal sampling: Suggest improvements

## Slide 43
43
Raw meal sampling: Suggest improvements
Sampler is located here

## Slide 44
2015-08-04
44
Cement sampling: Suggest improvements
Sampler
Sample container

## Slide 45
45
Hot meal sampling: Suggest improvements

## Slide 46
46
Powder sampling: suggest improvements …

## Slide 47
47
Clinker sampling: Not recommended