## Slide 1: Material Size reduction Crushing, screening and impact on grinding
SPREAD 2016-2017, Settat May 2016

## Slide 2
2
Process Overview
Material chemical homogeneity
Material size reduction…
Material moisture reduction
Material handling

## Slide 3
3
… First step, the material extraction. Generally we talk about drilling & Blasting …
Drilling &
blasting
Product size after the blasting is defined by:
  Geology
  Drilling & blasting procedure
  Loading equipment type
  Crusher type & size

## Slide 4
4
…Second step, crushing & screening…
Crushing & screening
Product size after the crushing system is defined by:
  Raw mill type / size
    0/30 - 50 mm for a ball mill
    3% - 5% of roller mill diameter
And influenced by
  Crusher feed size
  Type of crushing system

## Slide 5
5
…and the last step,the raw mill system …
Grinding
Product size after the raw mill is defined by:
  Raw meal burnability

## Slide 6
6
Energy Efficiency of Blasting, Crushing and Grinding vary in a large range and optimum balance in case by case based...
Blasting
h %

## Slide 7: …balancing energy inputs and cost for size reduction from the blast to the kiln feed…
Optimize energy distribution blasting, crushing & grinding
Wear part management
Improve raw/cement mill
feed size
…as well as wear parts cost for crusher / raw mill …

## Slide 8: A systemic approach has been grouped in four pillars aiming to secure the sustainability and efficiency of the operations from the quarry to the kiln feed…
LafargeHolcim Mining Community
… and the subsequent impact on the downstream processes…

## Slide 9: 400 Mio. t/a1) of raw material are blasted, crushed and ground in order to produce raw meal for the kiln for a total spending of about 2’000 Mio. CHF/a
Blasting
Crushing
Drilling
Loading & Hauling
Raw Meal Preparation
750
350
900
Current Cash Cost in Mio. CHF/a
Raw Material Extraction
Grinding
1) Initial estimation excluding China, additionally, includes about 100 Miot/a waste
Raw Material Preparation

## Slide 10
Experiences show that increasing the energy input by blasting leads to an improvement of the Crushing and Grinding processes
Blasting
Crushing
Grinding
0.2 kWh/t
2.0 kWh/t
20 kWh/t
0.3 kWh/t
1.8 kWh/t
18 kWh/t
-14 Mio. CHF/a
3 Mio. CHF/a
32 Mio. CHF/a
Actual
Future
Savings
Investing more

## Slide 11
11
Material Size reduction – 1st Step EXTRACTION  BLASTING

## Slide 12: Size reduction starts in the quarry. Different raw material extraction methods are used….

## Slide 13
13
Blasting depends on many parameters…
…combined with explosive type and blast sequence
Do you want to see a blasting?

## Slide 14
14
…and possibilities to improve its outcome, the fragmentation..…
Normal
Optimized

## Slide 15
15
… playing a key role on influencing the performance of the 2nd size reduction step; the crushing.
The crushing feeding strategy depends mainly of the crusher physical dimensions (e.g width, roller diameter, depth, etc.)
* data according to Sandvik

## Slide 16: Material Size reduction – 2nd Step CRUSHING

## Slide 17
17
The cement crusher portfolio
Abrasiveness
Stickiness
Primary
Hardness
Secondary
Roller
Sizer
Impact
Double
Hammer
Gyratory
Jaw
Single
Hammer
Process
Coarse
Wear Rates
Moisture
Moisture
Compressive
Strength
Scalping
> 6 months life
< 6 months life
>200MPa
<200MPa
<150MPa
8
–
12%
>12%
>8%
<8%
<8%
Fines
Decision Tree for Crusher Selection

## Slide 18
18
The crusher portfolio in Legacy Holcim

## Slide 19
…regardless the type the crusher goal is always the same….
Crushing goal: Provide the adequate feeding in terms of size in a stable mode to the raw grinding.

## Slide 20
20
… the crusher product size is mainly impacted by the feeding (reduction ratio, RR) & the crushing settings. The stability of the product size by the crushing tools wear management ……
Impactor
Hammers
with grate
Secondary
Primary
Compressive crushers
(giratory, jaw, cone)
Sizers & roller crushers
10:1
15:1
< 50:1
--
< 5:1
< 5:1
3.5:1
3:1
4:1
6:1
YES
YES
YES
NO
YES
Settings Adj.
The larger the reduction ratio the lower the production rate and the crusher product PSD more distorted (max size and intermediate sizes).
Adjustment of crusher settings allow to compensate the impact of wear in the crushing tools (bars, hammers, teeth) maintaining constant the crusher product PSD.
Redu. Ratio

## Slide 21
21
Criteria for Crusher Selection
Feed size and product size related through the Reduction ratio
Example: Feed size X: 1500 mm
Product size Y: 60 mm
Total Red. Ratio = 1500/60 = 25:1
RR_I primary crusher = 3:1
RR_II secondary crusher = 3:1
Two-stage crushing= RR1 x RR2 = 9:1
not sufficient ,3rd crushing stage required !
RR_III tertiary crusher = 3:1
Three-stage crushing= R1 x R2 x R3
> Total reduction ratio: 27:1

## Slide 22
22
Crusher feed size definition / options
Feed size
1.131
1.4

## Slide 23: … How do you assess this crusher performance?
Luga It – Phillipines
Double Roller Crusher
Limestone
2015 Performance
Weekly Averages

## Slide 24: ….. Would you say the same now?
Luga It – Phillipines
Double Roller Crusher
Limestone
Random shift during 2015
Hourly Averages

## Slide 25: What would you say on the performance of this Crushers?
Langkawi – Malaysia

## Slide 26: … what about adding a bit more of information?
Langkawi – Malaysia
Single Shaft Hammer
Limestone
2015 Performance
Monthly Averages

## Slide 27
27
A crushing system is considered as high performing when produces, in a sustainable way, the desired sizes at maximum production rate at the lower cost.
Overall the performance in a crushing system is impacted by:
Material characteristics
Feed strategy (homogeneous & choke)
Operator efficiency
Crusher internals (rotor speed, rotor configuration, crushing tools shape)
Crusher settings management & crushing tools wear management
… but what is then a high performing crushing system, and what is influencing it?….

## Slide 28
28
Soft material
  Finer granulation
  Increased crusher capacity
Hard material
  Coarser granulation
  Reduced crusher capacity
The Influence of the material characteristics
Impact Crushers
The type of crushed material affects crusher capacity and product PSD

## Slide 29: The Influence of the Feeding Strategy

## Slide 30: Blasting fragmentation is not exactly crusher feeding
Loading is a key process for crusher performance!!!!
Feeding strategy is not only targeting a maximum feed size is targeting an, as much as possible, homogeneous feed.

## Slide 31: The adequate feeding strategy is….
Homogeneous in size distribution truck by truck with a clear defined target in maximum feed size.
Sufficient to maintain a choke feeding to the crusher
Consult the quarry colleagues
Efficient loading operators.
Blasting muckpile cut strategy (“pre-blending mode if feasible”).

## Slide 32: The influence of the Crusher Operator Efficiency
  Process control system (Instrumentation)
      Belt scales (t/h)
      Counters (hours, power, amperes)
      Sensors (Vibrations, bearing temperature, speed, hopper level)
  Senses
      Visual contact with feeding (direct or camera)
      Noise of the equipment
      Smell (V-Belts burning)
  Information from the quarry
And, normally just counts with the possibility to change the feeder speed for increase or decrease the production rate.

## Slide 33: The influence of the crusher internals. Which parameters can we control and handle to guarantee a high performing crusher?
  The settings; breaking plates, grates, gaps, anvils (All crusher types but sizer which is not adjusted mechanically).
  The cleaning devices (Roller crusher, Sizers).
  The crushing tools; hammers design, bars design, teeth design, teeth pattern, etc. (All types).
The material distribution onto the crushing tools; feeding geometry, chutes, feed plates; (All crusher types).
The rotating speeds ; rotors, rollers, fly wheels, etc(All crusher types).
The eccentric strokes (gyratory crushers/ jaw crushers / cone crushers).
Daily managed
Requires expert intervention (CIP) and expenditure

## Slide 34: The settings management
  The crusher settings defines the crushing chambers inside the crushers.
  They have to be adjusted based on the product size target and the feed size.
  Generally by reducing the crushing settings (gap between rollers, breaking plates, grate to hammer distance, grate slots dimensions, close side setting, etc) you can expect, assuming same feeding strategy (same size and choke)
        Lower production rate.
        Higher wear rate.
        Finer granulometry (intermediate sieves in the curve)

## Slide 35: The settings management - Impact crusher
Side plates
Breaker plates
Rotor
Bars/Hammers
Grinding path
Inlet chute
Feeding plate

## Slide 36
S1
S2
S4
Fmax: Maximum feed size
S1~ (Fmax + P100*)/4 + 20 mm
S2~ S1 / 2 to 2.5
S2 > Fmax /10
a
S3
S3~ S2+ 10 to 20 mm
S4 ~ P100 - 10 mm (Hazemag) or Using Typical Curves (Metso)
If no S3 & S4; Pmax ~ 1.6 S2
Coarser product in range 1mm – 10 mm with larger S1 and S2
The Impact Crusher Settings. Rules of thumb (Mix of Metso & Hazemag)
* The expected Product Size targeted (e.g. 0-40 mm  P100 = 40 mm

## Slide 37
37
The effect of the settings in PSD curves. The manufacturer Typical PSD (Metso)

## Slide 38
38
The settings management, the Hammer Crusher
Single Shaft Hammer Crusher

## Slide 39: The settings management, the Hammer Crusher
Breaking Plates
Grate Slots
Hammer to grate distance
Hammer to anvil distance (anvil and hammer wear)
Hammers
Double Hammer Crusher

## Slide 40
40
Replacement of outlet grate (shift in / out) only option for product max size control.
Some models have an adjustable grate to compensate wear of the hammer heads (Rule of Thumb -> Distance = 90% Grate slot width). Increase of distance reduce production rate increasing wear.
For hammer crushers, there are various designs available, basically the size control is achieved through the opening of the outlet grate

## Slide 41
The grate is key for the max product size, the breaking plate for the granulation
8,5 cm
6 cm
3 cm
9 cm
30,5 cm
10 cm
The breaking plate distance to hammer provides the possibility to have an overall finer product granulation or coarser. Production rate is thus, affected.

## Slide 42
42
The effect of the settings in PSD curves. The manufacturer Typical PSD (FLS EV hammer crusher family & ThyssenKrupp)

## Slide 43
43
Only as primary stage
Product with little fines
CSS/OSS adjustments range depends on machine size
Secondary stage made with a cone crusher of hammer crusher
Crushing chambers always as full as possible to avoid fishy product and allow maximum utilization of liners
The settings management; compressive crushers
200 – 900 t/h
Pmax= 1.3 – 2.5x CSS
Product: 80%PCSS
600 – 8’000 t/h
Pmax= ~ 2 x OSS
Product: Target = OSS

## Slide 44
44
For hard abrasive rock
Does not require a feed hopper
Can be choke fed from two sides
Largest acceptable feed = Feed opening x 0.9
Feed in direction of spider arms for material distribution
The setting management; the gyratory crusher
42
65
Feed
Opening
Nomenclature example: 42-65
- 42’’ feed opening
- 65’’ largest shaft diameter

## Slide 45
45
With screw
With hydroset
Gyratory crusher settings

## Slide 46
The effect of the settings in PSD curves. The manufacturer Typical PSD (Metso)

## Slide 47
47
For secondary / tertiary applications
Two types
  Hydrocone
    Basically a small gyratory crusher
  Symons type
    Different movement & setting
Cone crusher types
Cone

## Slide 48
48
Symons type cone crusher
Cone

## Slide 49
49
Typical design of a cone crusher, example for HP crusher type from Metso
Pmax= 1.3 – 2.5x CSS
50 – 800 t/h
Product: 80%PCSS
CSS

## Slide 50
The effect of the settings in PSD curves. The manufacturer Typical PSD (Metso)

## Slide 51
51
The setting management; Double roller crusher

## Slide 52
The setting management; Double roller crusher
Pmax= 1.2 – 1.3 x Gap
Product: 80%Pgap

## Slide 53
The effect of the settings in PSD curves. The manufacturer Typical PSD (Sandvik)

## Slide 54
54
Roller crusher production rate versus dimensions, example for FLS machines

## Slide 55
55
Settings are defined from manufacturing. Crushing tools wear management is the key to keep both production rate and product size.
The setting Management – The mineral sizer

## Slide 56
What else can be done to increase the production rate or influence the product granulometry? Impact Crusher
Fine feed
Coarse feed
Rotor speed can be adjusted but always > 20 m/s (referred to the number of blow bars).
Recommended speed in the range of 30-36 m/s (StDC)
Higher speed are feasible but after consultation with CIP.
Flatter inlet chute = coarser product. e.g a from 60° to 40° 35%P1mm to 20 %P1mm
Feed even along the rotor width  uneven wear impacting the production rate and the wear costs.
Choke feeding  underfeed leads to uneven wear, low production rate and distorted granulometry.
Slotted Rotor  Special configuration. Never without consulting CIP

## Slide 57
Recommended speed in the range of 30-36 m/s (StDC)
Higher speed are feasible but after consultation with CIP.
Feed even along the rotor width  uneven wear impacting the production rate and the wear costs.
Choke feeding  underfeed leads to uneven wear, low production rate and distorted granulometry.
Progressive grate design when clogging effect in the grate occurs – Higher stickness of the material.
Segmented grates for quick exchange.
What else can be done to increase the production rate or influence the product granulometry? Hammer Crusher

## Slide 58
Rotational speed is given and to challenge it a significant change in the material characteristics is expected. Consultation with CIP
Choke feeding  underfeed leads to uneven wear, low production rate and distorted granulometry
What else can be done to increase the production rate or influence the product granulometry? Gyratory Crusher
Increasing the eccentricity  Bigger stroke lead for more production rate. Consultation with the CIP

## Slide 59
What else can be done to increase the production rate or influence the product granulometry? Hydrocone & Symons Crusher
Rotational speed is given and to challenge it a significant change in the material characteristics is expected. Consultation with CIP
Choke feeding  underfeed leads to uneven wear, low production rate and distorted granulometry
Increasing the eccentricity  Bigger stroke lead for more production rate, better product shape.
The interchangeable crushing cavities are the most common way to adapt the crusher to new feed conditions or new product sizes requirements. Expenditure is associated and normally is never done. Consultation with CIP is a must.

## Slide 60
What else can be done to increase the production rate or influence the product granulometry? Double Roller Crusher
Feed even along the rotor width  uneven wear impacting the production rate and the wear costs.
Choke feeding  underfeed leads to uneven wear, low production rate and distorted granulometry.
The cleaning scrapers guarantees higher production rate as maintains the rollers gap by removing buildups from the inter teeth channel
Recommended speed in the range of 5-7 m/s (StDC)
Possibility to reduce one roller speed to increase shearing effect  gaining production rate in cases of high stickiness of the material

## Slide 61
What else can be done to increase the production rate or influence the product granulometry? Mineral Sizer
Recommended speed in the range of 2-3 m/s (StDC)
Higher/lower speed are feasible but after consultation with CIP. Expensive with Spur Gears
Teeth pattern  e.g. 4 x 6 to 3 x 8 for scroll pattern. Granulometry is expected also coarser
Different teeth height  Grabbing oversized
Addition of a breaker anvil
Timing of the rollers when scroll teeth pattern
The cleaning scrapers guarantees higher production rate as maintains the rollers gap by removing buildups from the inter teeth channel

## Slide 62: Assessing a crusher system

## Slide 63
63
Blockages due to oversized feed
Crusher plugging due to material stickiness
Low transport capacity of conveying system after crusher (e.g. SH, DV, MG, etc.)
Variations of rock hardness (UCS)
Low capacity of mobile fleet
Wear of crushing tools lead to loss of product size
Generally, crushing is performing far below nominal capacity and affect the performance of the raw mill but as well as the one of the quarry operation.

## Slide 64: Crusher system assessment scope
Production
  Production Volumes
  Energy Consumption
  Crusher Product Size
  Wear
Operational
  Operating hours
  Production Rate (BDP)
  Workflow procedure
    System Availability
      Downtime & Idle Time
The crusher assessment shall answer questions like:
Why the production rate is lower than BDP? Can I increase it?
Can I reduce the it energy consumption of the system?
Is the product homogeneous and in target? Can I improve any condition?
Is the wear cost optimize? Can I reduce it?
In the feeding Is the production rate the maximum to achieve?
The scope of the assessment must cover two main streams; Operational and Production which often cross among them.

## Slide 65: Define the boundaries of your assessment
Crusher
System Limits
Downstream process
Upstream process
Source: Garadagh Crushing System

## Slide 66: Set a base line  Start to formulate questions
Recommended a year, monthly average.

## Slide 67: Set a base line  Analyze the crusher setting and target working conditions, compare to the design  Keep asking questions
What are the reasons for a change on Maximum Feed Size?
What are the reasons for a change on rotor speed?
What current setting strategy is based on?
When were set the current BDPs?
How long since adjustments for the inspection?

## Slide 68
68
Field observation under regular operational conditions  Sit on the Crusher CCR for a day, observe and record  Keep asking questions
Observation
Analyze the feeding.
Is granulometrically homogeneous?  All dumps look similar in hopper
Is continuous?
Try to estimate PSD of the feeding  Picture PSD Analysis (Visiorock, Wipfrag, Split Engineering) in hopper and blasting muckpile for comparison.

## Slide 69
69
Field observation under regular operational conditions  Sit on the Crusher CCR for a day, observe and record Keep asking questions
Observation
Analyze the effectiveness of the PID control loops if there are.
Observe the Operator routines for crushing monitoring and control.
How is the communication between crushing, quarry, CCR or Pre-Blending?
Record operational data: Crusher throughput, absorbed power, downtime and its causes, idle time and its causes.
Calculate & Compare:
Specific energy consumption
Gross Production rate
Availability
Effectiveness (OEE)
Net Production rate

## Slide 70
70
Take samples under regular operational conditions
Material Sampling for:
Product size analysis.
Reduction Ratio Analysis
Screens efficiency analysis.
* Make sure the crusher settings status is known to be able to link the results to them

## Slide 71
71
When Sampling….. remember
Sample size must be adapted to maximum grain size in order to be representative
Sampling from belt conveyor after a system crash stop

## Slide 72: Gross Production rate vs Net Production Rate (Utilization factor)
Crusher running with & without feeding (Crusher hour meter)
Crusher running with feeding (feeder hour meter)
Net Production Rate
x 100

## Slide 73
73
Crusher visual inspection
Impact plates position. Measure
General wear observation
Grinding path position measure
Feeding plate, braking plates, rotor ribs
Do you see anything that explains/answers the questions done before?
*The inspection should be done close in time to the field observation.

## Slide 74: Crusher system assessment results
After measurements, inspection, monitoring and investigation we are able to answer our questions:
Why the production rate is lower than BDP? Can I increase it?
Can I reduce the it energy consumption of the system?
Is the product homogeneous and in target? Can I improve any condition?
Is the wear cost optimize? Can I reduce it?
In the feeding Is the production rate the maximum to achieve?
An prepare a action plan to correct or improve whatever finding:
Setting adjustment calendar (To increase the product size homogeneity)
Reduce maximum feed size (To increase the production rate)
Adjustment of the control loops (To reduce lack of feeding in crusher)
Or set trials for new product size target (finer).

## Slide 75: Size Reduction Initiative

## Slide 76
Mine to Kiln (M2K)
SRi
Initiative n
Initiative n-1
Mining Performance Booster
Data source* to analyze potentials of a plant / a region
KPI’s* to analyze current data, but also track progress of implementation
Tools* / templates* to: calculate potential of initiative, track progress of implementation, reporting
Establish a clear process with roles and responsibilities
Training*
Others*
A Global Initiative is a program of projects that aims to improve performance/cost by addressing common challenges identified through benchmarks and analysis and lead to finally sustainable and continuous improvement within the daily operations.
* … exists or have to be developed

## Slide 77: …balancing energy inputs and cost for size reduction from the blast to the kiln feed…
Optimize energy distribution blasting, crushing & grinding
Wear part management
Improve raw/cement mill
feed size
…as well as wear parts cost for crusher / raw mill …

## Slide 78: …. because a better performance in the raw mill affects the upstream processes …
Crushing Assessment
MF Site Assessment
Drill & Blast Assessment
Raw Mill Assessment

## Slide 79: Coordination - cooperation mines / production – process / maintenance is a key parameter for capturing identified benefits
Capturing benefits is the drill / blast / load / haul operations
Improved specific energy consumption of crushing
Improved efficiency of the raw mill (electrical consumption)
Improved reliability of the raw mill (higher MTBF, lower probability of gearbox failure by vertical roller mill)
Benefits for all involved

## Slide 80
80
Impact of feed size on raw mill performance is a fact
DS  1.2 kWh/t
HN  2.2 kWh/t
GU  1 kWh/t
LN  0.9 kWh/t
There are much more experiences:
Mabini
Wadi
Malagueño
Tecoman
Ternate

## Slide 81
More recently….
Luga It January 2016
Kantaan April 2016

## Slide 82: …Techport study along 2015, after the SRi Workshop at Wadi shows estimated benefits in the range of 930 kCHF/a for the identified focus plants …
Pilot SRi Workshop 2015 / 410 kCHF (+)
SRi Workshop 2016
2018, new quarry
2017, new fleet
2017
2017, new quarry
…for the 1st large scale project for the SRi…

## Slide 83: The developed simulator allows better definition of the business cases with the aim to foster the feed size optimization to the raw mills
Foster own plant initiatives as OZ, MG, CG, HR
Link also cement mills (GU, NO): e.g. N1&2 + 21% production rate as per LST feed size optimization
Foster utilization of alternative suppliers (e.g. Vega) to CIP and higher technology wear parts (e.g. Martensitic steels, ceramic inserts)
DMI WS at Wadi done for spreading the initiative to India

## Slide 84: …now that we did the crusher assessment we can estimate impact of change of feed size in the raw mill…
The model is based on a simple and demonstrated fact “The decrease of specific energy consumption in the mill motor is linked to the increase of specific energy consumption in the crusher upstream”.
Exactly the new Mill SEEC will be the Existing minus the increase of Crushing specific energy consumption times a Bonus Factor
The bonus factor calculation is based in demonstrated cases.
So… by estimating the new crushing energy consumption when reducing the product size we will be able to estimate mill motor and system new energy consumptions and also crusher system energy consumption.

## Slide 85
85
…… let’s do an example with an impact crusher
Current Crusher Settings:
P90% = 80 mm
Target Crusher Settings
P90% = 50 mm

## Slide 86
86
Impact of feed size on raw mill performance

## Slide 87
87
Influence of crusher setting (IC) on kWh/t for the crusher
According to Metso crusher specific energy consumption increases drastically with end product sizes
1.1 kWh/t
0.87 kWh/t

## Slide 88: Basics on Screening
Technical Development Program for PPE 2015-2016

## Slide 89
89
Operating Principle and Design Features
Fine Fraction
Product
Coarse Fraction
Tailings
Feed (A)
Fines (F)
Rejects(R)
Screen
Terminology of Separation Process
(note that different words are used for the same)
Incoming Flow

## Slide 90
90
Deck length defines quality
Deck width defines capacity
Principle of screening
Factors affecting stratification
  Material characteristics
  Bed height
  Slope
  Stroke characteristics

## Slide 91
91
Motion: Linear or circular
Single or multiple decks (to produce various fractions)
Wobbler screens for sticky material
Screening equipment

## Slide 92
92
Scalping: removal of fines before crushing
Application in open circuit crushing system

## Slide 93
93
Control of top grain size
Application in closed circuit crushing system

## Slide 94
94
Factors affecting screen performance & efficiency
  Feed material
  Motion type
  Feed rate
  Feed point (material distribution on deck)
  Screen size
  Screening media
  Screen inclination
  Opening shape
  Stroke
  Frequency
Screen performance & efficiency

## Slide 95
95
Screening Efficiency & Quality
Coarse material in fine fraction
Due to wear or holes
Due to fishy particle shape
Fine material in coarse fraction
Due to clogged screen
Due to low efficiency
Due to screen saturation
 Goal: < 20 % fines in coarse