## Slide 1: Clinker Characteristics and Burning Behavior
PPE Course

## Slide 2
2
Provide understanding for the relationship between raw meal, fuel and clinker characteristics and burning behavior
Provide guidelines for appropriate ranges of chemical moduli and minor elements
Present tools for assessment and optimization of burning behavior and clinker properties respectively reactivity
Objectives

## Slide 3: Agenda
Clinker Formation and Burning: A short Overview
5
Appropriate ranges of chemical module and minor elements
17
Burnability test: Application for Raw Mix Optimization
35
Clinker Granulation and Coating Formation
48
Clinker Microscopy: A Diagnostic Tool
62
Conclusions
69

## Slide 4: Clinker Formation and Burning: A short Overview

## Slide 5
5
Quasi Quantitative Variation of Minerals with Temperature
Free Lime
Alite
Belite
Aluminate
Ferrite

## Slide 6
6
Sequence of Reactions Occurring in a Rotary Kiln System
Heating (°C)
20 - 100 Evaporation of H2O
100 - 300 Loss of physically adsorbed water
400 - 900 Removal of structural H2O (H2O and OH groups) from clay minerals
>500 Structural changes in silicate minerals
600 - 900 Dissociation of carbonates
>800 Formation of belite, intermediate products, aluminate and ferrite
>1250 Formation of liquid phase (aluminate and ferrite melt)
~1450 Completion of reaction and growth of alite and belite
Cooling (°C)
1300 - 1240 Crystallization of liquid phase into mainly aluminate and ferrite

## Slide 7
7
T [°C] | Type of Reaction | kJ/kgclinker | 
0 - 1450 | Heating of raw materials | » | 2050
400 - 900 | Dehydration of clays | » | 170
600 - 900 | Decarbonization of calcite | » | 1990
> 800 > 1250 for Alite | Heat of formation of clinker minerals | » | - 420
> 1250 | Heat of melting | » | 105
 | Crystallization of dehydrated clay | » | - 40
1300 - 1240 | Crystallization of melt | » | - 105
< 1240 | Cooling of clinker | » | - 1'400
 | Cooling of CO2 (ex calcite) | » | - 500
 | Cooling of H2O (ex clays) | » | - 85
Net theoretical heat of clinker formation |  |  | + 1765
Clinker Formation: Energy requirement (dry process)

## Slide 8
8
In addition to the clinker formation process, several additional chemical and physical reaction take place in the kiln system.
Burning Behavior

## Slide 9
9
 | Raw Meal Chemical Composition Fineness Microhomogeneity Uniformity | Fuel Ash Content and Composition SO3 Contents Operational Conditions Production Rate Temperature Profile Residence time Dust Return Uniformity of Operation: Kiln Feed Fuel Rate Gas Rate
Kiln System Type of: Kiln, Preheater Precalciner, Cooler Dimensions Heat exchanger Refractory Lining | BURNABILITY BURNING BEHAVIOR | 
Burning Behavior

## Slide 10
10
Acts as a solvent (transport medium) and facilitates Alite formation
Enables clinker granulation
Enables coating formation (but also ring formation)
Significance of Liquid Phase

## Slide 11
11
Most raw mixes show similar minimum temperature of liquid formation (eutectic point), but the quantity of liquid formed at which temperatures varies with raw mix chemistry.
For OPC clinker, the eutectic melting point is at 1338°C; the composition of the liquid is:
CaO - 55 %
SiO2 - 6 % Alumina ratio
Al2O3 - 22 % (AR) = 1.38
Fe2O3 - 16 %
Liquid Phase

## Slide 12
12
Calculation of Liquid Phase Quantity
Formulae for quantitative calculation acc. to LEA
  1338 oC = 6.1 Fe2O3 + MgO + Na2O + K2O if AR  1.38
      8.2 Al2O3 – 5.22 Fe2O3 + MgO + Na2O + K2O if AR 1.38
  1400 oC = 2.95 Al2O3 + 2.2 Fe2O3 + MgO + Na2O + K2O for MgO  2%
  1450 oC = 3.0 Al2O3 + 2.25 Fe2O3 + MgO + Na2O + K2O for MgO  2%
Typical calculated quantities at 1400 °C: 20 to 30 %
% liquid phase | Characterization
< 23% | dry
23-27% | normal
> 27% | wet

## Slide 13
13
Amount of Liquid: Effect of Chemistry
10
15
20
25
30
35
1338
1400
1450
°C
%
LA
TR
MI
CA
SR = 2.04 AR = 1.44
SR = 3.29 AR = 1.33
SR = 2.48 AR = 2.49
SR = 2.53 AR = 0.93
AR indicates the amount of liquid formed early, at relatively low temperatures (max at AR 1.38)

## Slide 14
14
Amount of Liquid: Effect of Chemistry
SR indicates the final amount of liquid formed (higher SR = less liquid)

## Slide 15
15
Data from Holcim Industrial clinkers (Product handbook)
Quantity of Liquid Phase: Correlation with SR

## Slide 16: Appropriate ranges of chemical module and minor elements

## Slide 17
17
Chemical Moduli in Holcim Clinker (ATR 2014)

## Slide 18
18
Chemical Moduli in Holcim Clinker (ATR 2014)

## Slide 19
19
Industrial clinkers concentrate in the following range of chemical moduli (Like-For-Like)
A normal burning behavior and clinker quality can be expected from clinkers within this range.
Clinker Chemical Moduli
Moduli | Typical range | avg ATR 2002 | avg ATR 2010 | avg ATR 2012
LS | 94 – 98 | 96.0 | 95.4 | 96.0
SR | 2.35 – 2.75 | 2.58 | 2.50 | 2.53
AR | 1.4 – 1.8 | 1.58 | 1.50 | 1.50

## Slide 20
20
Deviations from the ‘normal’ ranges can be due to:
  Need for high clinker strength potential to maximize clinker substitution or to meet market needs:
    LS > 98, SR > 2.75, AR > 1.8 (+/- mineralization)
  Plant specific optimization of burning behavior
  Specific composition of main raw mix components
    Lack of correctives, minimization of components
    Shortage of sufficiently high grade limestone
    In case of unsatisfactory burning behavior or quality: search for correctives, incl. AR
  Limit of C3A content (Sulfate-resistant cement): AR < 1.4
Clinker Chemical Moduli (cont)

## Slide 21
21
Typical ranges for mineralized clinker:
  LSF: 101 –103
  SR: 2.6 – 3.0
  AR: 1.6 – 2.0
  C3S: > 70% (Bogue); > 75% (Microscopy)
  Liquid phase: 23 – 25%
  F: 0.23 ± 0.02%
  Free lime: < 2%
Kiln feed burnability (according to Holcim test):
  Moderate to good
Design of mineralized clinker (Holcim Method)

## Slide 22
22
The addition of F improves clinker burnability. This effect can be exploited by increasing the LS of kiln feed to achieve very high alite contents in clinker.
F is typically sourced from natural fluorspar. Alternative sources can be spent cell liners (SPL).
Possible benefits which can be obtained from such more reactive clinker are as follows:
  Decrease of clinker factor
  Reduction of cement production costs
  Improvement of cement quality
  Increase of cement production volume (at constant clinker capacity)
  Reduction of specific CO2 emissions
  Improved SO3 incorporation
Clinker mineralization with fluoride facilitates the production of clinker with alite contents up to 80 %

## Slide 23: Mineralizers
“Mineralizers change the chemical potential G of the reactants: when the mineralizer enters into solid solution of the educts the rate (of the forward reaction) is decreased, when it enters into solid solution in the product the rate is increased.”
Most of impurities are more soluble in belite than in alite
But F is more soluble in alite than in belite
Substitution of O by F in the crystal lattice of alite increases disorder and thereby improves hydraulic reactivity

## Slide 24
24
CaO SiO2
G
CaO C3S C2S
G
CaO SiO2
CaO F-C3S C2S
Chemical potential of pure CaO, C2S and C3S at 1100° C
Chemical potential of CaO, C2S and F-containing C3S at 1100° C
CaO and C2S stable at 1100° C
CaO and C3S stable at 1100° C
C3S and C2S stable at 1100° C
Principle of F-mineralization - thermodynamics

## Slide 25
25
Mineralizing effects of F - kinetics
Increased rate or reduced temperature by F addition
Reaction Rate

## Slide 26
26
Example: Clinker microstructure Saraburi 1
normal
mineralized

## Slide 27
27
Chart: Comressive Strength (MPa)
| 2 Days | 7 Days | 28 Days
Baseline | 19.1 | 31.5 | 42.7
Mineralized | 24.3 | 37.1 | 48
Mineralized (reduced clinker factor) | 19.6 | 33.2 | 44.4
Visualizing Improved Clinker Factor (e.g. Fès)
+27%
+18%
+12%
-4% clinker
-4% clinker
-4% clinker

## Slide 28
28
Challenge: F acts as a set retarder

## Slide 29
29
Good preparation of an industrial mineralization trial is crucial
  adequate dosing system
  uniformity of fluorspar is more important than its purity
  calibration of XRF for new clinker composition (higher LS)
F analysis is possible by ion selective electrode (ISE) and XRF, but not trivial
  critical for ISE are sample dilution (matrix effect) and correct calibration when using direct measurement
  critical for X-ray fluorescence is the calibration with plant specific standards
Good condition of kiln system is also important for burning of mineralized kiln feed
  preheater efficiency (false air) and cleaning
  impact of bypass operation
Experiences from industrial trials

## Slide 30
30
With increasing petcoke utilization, SO3 in clinker is often very high
(>> 1 %)
SO3 incorporation in clinker is facilitated by availability of alkalis:
  Traditionally molar A/S ratio: ≥ 0.8, now < 0.5 is common!
At low molar A/S ratio (< 0.8)
  SO3 can be incorporated in Ca2K2(SO4)3
  SO3 can be incorporated in belite
  Remaining SO3 then forms anhydrite (CaSO4)
Possible consequences:
  Reduction in alite content in clinker (SO3 stabilizes belite and retards belite conversion to alite) and therefore clinker reactivity
  Need to adjust addition of soluble sulfate in cement (extreme cases)
SO3 and Alkalis

## Slide 31
31
The form and distribution of sulfate in clinker is affected by the total percentage of SO3 in clinker and by the alkali/sulfur ratio.
Distribution of SO3 in clinker phases
A/S = 1
A/S > 1
A/S < 1
Arcanite
Aphthitalite
Ca-Langbeinite
Anhydrite
Orthorhombic
aluminates
Aluminates = C3A
Arcanite = K2SO4
Apthithalite = (K,Na)2SO4
Ca-Langbeinite = 2 Ca2SO4*K2SO4
Anhydrite = CaSO4
Quality issues
Process & Quality Issues

## Slide 32
32
Among silicates, belite builds significantly larger amounts of sulfur into its crystal structure compared to alite. Up to 4-5 times more SO3 can be incorporated into belite compared to alite.
In the absence of alkalis and MgO, sulfates jointly with alumina are integrated into belite. This leads to
  A decrease of the aluminate content
  Stabilization of the belite and a reduced formation of alite
The incorporation of S6+ into belite can increase the belite content at the expense of alite by as much as 10-15 wt%.
High SO3 content further reduce alite be absorption of CaO (Ca-langbeinite, anhydrite in extreme cases)
Quality issues related to high sulfur content in combination with low A/S

## Slide 33
33
Influence of SO3 on Aluminate content
Chart: "Free" SO3 [%]

## Slide 34: Burnability test: Application for Raw Mix Optimization

## Slide 35
35
Burnability: How easy clinker forms
Burnability influences:
  Kiln operation (heat consumption, refractory wear, volatility)
  Degree of clinker burning and therefore reactivity of clinker
Burnability can be assessed by laboratory burnability tests
  Determine optimal raw meal fineness
  Determine main factors contributing to burnability
Burnability is primarily influenced by
  LS and SR
  Coarse quartz: > 32 µm
  Coarse calcite: > 90 µm
A direct relationship between raw meal fineness and burnability is not mandatory
Raw Meal Burnability

## Slide 36
36
The test is based on the isothermal burning at 1400 °C of raw meal nodules
The test allows the determination of the relative influence of the various material parameters, free from the influence of process technological disturbances.
Evaluation Free Lime %
  very good 0 - 2
  good 2 - 4
  moderate 4 - 6
  poor 6 - 8
  very poor > 8
Holcim burnability test

## Slide 37
37
Hocim Burnability Test

## Slide 38
38
Calculation of the CaOf-content, as expected to result from the burnability test, according to the formula:
with calculations for: LS = lime saturation SR = silica ratio Cc = percentage of critical calcite > 90 microns Q = percentage of critical quartz > 32 microns
Physiochemical Burnability Model
CaOf = 0.56*Q>32 mm + 0.166*Cc>90 mm + 0.356*LS + 0.804*SR - 33.886

## Slide 39
39
Example of Physiochemical Burnability Model
Raw Meal Burnability
0
1
2
3
4
5
6
7
8
9
10
Rating
2002 Test
2002 Model
2003 Test
2003 Model
% free lime
test
Quartz > 32 mm
Calcite > 90 mm
Chemistry
LS = 95.7
SR = 2.85
AR = 1.79
R90mm = 12.7%
Very Good
Good
Moderate
Poor
Very Poor
LS = 96.9
SR = 3.11
AR = 1.81
R90mm = 13.8%
Test 1
Model 1
Test 2
Model 2

## Slide 40
40
Burnability test: Industrial meals 2000 - 2015

## Slide 41
41
Situation
  Wet process plant; excessively hard burning to drive off alkalis for meeting low-alkali requirement results in low-reactive clinker
  Presently 2-component mix (limestone, shale), Na2O-equiv. = 1.0 % (clinker basis)
  Intention to modify mix by using additional components – in particular AR - to lower alkali level. This should allow softer burning and yield higher clinker reactivity.
Burnability: Mix Optimization Example 1

## Slide 42
42
  Possible mixes are:
Question What is the difference in burnability between the mixes with silica gel and silica dust respectively?
Burnability: Mix Optimization Example 1
Components | Mix with silica gel | Mix with silica dust
Limestone | 76.3 | 76.4
Shale | 16.0 | 17.3
Silica gel | 5.8 | --
Silica sand | -- | 3.8
Pond ash | 0.5 | 0.5
Mill scale | 0.7 | 0.6
Bauxite | 0.7 | 1.4
LS (clinker) | 98.0 | 
SR (clinker) | 2.60 | 
AR (clinker) | 1.86 | 
Na2O-equiv. [%] | 0.75 | 

## Slide 43
43
Burnability: Mix Optimization Example 1

## Slide 44
44
Assessment
  Silica gel is a favorable, amorphous silica corrective, having no negative impact on burnability: recommended material
  Silica dust is crystalline quartz, negatively impacting burnability; should only be used as second choice
Burnability: Mix Optimization Example 1

## Slide 45: Example 2: Impact of raw meal fineneness
Coarser raw meal on R200 decreases burnability due to coarse quartz influence
Raw meal line 1
Raw meal line 2
LS = 95 – 96
SR = 2.28 – 2.33
AR = 1.61 – 1.64
R90 = 16.70
R200 = 2.97
R90 = 15.30
R200 = 0.95

## Slide 46
46
Example 2: Impact of raw meal fineneness and correctives
Chart: Raw Meal Burnability
| Rating | Mix 1 | Mix 1 | MPR | MPR | Mix 2 | Mix 2
very good | 0
good | 0
moderate | 0
poor | 0
very poor | 0
Burnability Test | 3.9 | 5.5 | 6.2 | 5.8
Quartz > 32 um | 0.8 | 1.3 | 1.6 | 1.1
Calcite > 90 um | 0 | 0 | 0.3 | 1.3
LS + SR | 3.8 | 4.1 | 4.8 | 4.3

## Slide 47
47
Plant example of energy and cost savings as a net result of increasing raw meal fineness
Example: Mix Optimization and Cost Savings

## Slide 48: Clinker Granulation and Coating Formation

## Slide 49
49
Liquid Phase: Viscosity
High Viscosity
Low Viscosity
Temperature
lower
higher
Alumina Ratio
lower
higher
K2O > Na2O (increased SR, LS)
Minor Elements
MgO < Na2SO4 < K2SO4 < SO3
(Cl, F)

## Slide 50
50
Diffusion rate of ions is faster in low viscous liquids, promoting alite formation (mineralizing effect, e.g. F or SO3).
High viscosity of the liquid phase improves the granulation (nodulization) of the clinker; low viscosity makes granulation more difficult.
Low viscous liquid phase infiltrates refractory linings faster, leading to premature failures
Effects of changed viscosity (qualitative)

## Slide 51
51
Influence of minor elements on viscosity
Higher viscosity
Lower viscosity

## Slide 52
52
Liquid phase: Surface tension
Temperature
higher
lower
  Low Surface Tension
  Minor Elements: SO3 > K2O > Na2O > MgO > P2O5
Very low AR
High Surface Tension
Better nodule formation, lower dust.
Less coating due to less wetting of brick surfaces.

## Slide 53
53
High surface tension has less tendency to adhere to refractory linings, thus produce less coating.
Low surface tension enhances ‘wetting’ of particles and promotes alite formation.
Decreased surface tension favors growth of large alite crystals
Effects of changed surface tension (qualitative)
High surface tension favors nodule formation and liquid penetration through pores (denser clinker nodules). The resulting clinker is coarser and less dusty.

## Slide 54
54
Coating formation is influenced by quantity (SR) and viscosity (AR) of liquid phase.
Coating formation: Overview
NORMAL
COATING
2.2
2.8
SR
2.5
- 1.6
- 1.9
- 1.3
AR
thick coating clinker ball or sinter ring formation (plenty of viscous melt phase)
thin coating refractories attack (plenty of fluid melt phase)
thin coating
(little of fluid melt phase)
very thin coating dusty clinker (little of viscous melt phase)

## Slide 55
55
Impact of dusty clinker
  Impairs kiln operation (heat transfer from flame)
  Impairs cooler operation (transport, overheating)
  Impairs clinker grindability
Chemical factors increasing tendency to dusty clinker:
  Low liquid phase content: < 23 % (SR > 2.8)
  High LS: LS > 98
  High SO3 content: SO3 > 1.3
  (Tentative values only, can differ in individual cases)
Clinker Granulation

## Slide 56
56
Clinker granulometry significantly impacts the production process
 | Very coarse clinker | Very fine clinker
Burnability | Center of grains difficult to burn | Poor heat transfer to center of clinker bed
Cooling | Slow cooling | Problems in cooler operation
Dust cycles |  | Enhancement of dust cycles
Availability | Crusher wear and blockages | Wear of cooler grates
Grindability | Hard to grind if ball charge not adapted | Hard to grind due to lack of thermal micro cracks

## Slide 57
57
Recommended sieves for granulation assessment: 1, 5, 8, 16 mm
Tentative criteria for dusty clinker: > 25 % passing 1 mm
Investigation of 16 industrial clinkers:
Clinker Granulation
Sieve opening (mm) | Passing (%) |  | 
1 5 8 16 | x 10.2 32.8 46.7 74.5 | min. 0.4 15.1 24.9 59.1 | max. 30.9 53.5 64.1 92.4

## Slide 58
58
Clinker Granulation

## Slide 59
59
Impact of clinker balls
  Excessive clinker temperatures at cooler outlet
  Cooler operation (blockages)
Chemical factors increasing tendency to ball formation
  High liquid phase contents (> 27 %) and high viscosity (AR > 2.2)
Besides chemical factors, clinker ball formation is very much related to process condition (burner settings, sulfur volatilization, etc.)
Clinker ball formation

## Slide 60
60
The plant reduced a silica rich alternative resource (contaminated soil)
To compensate for lower SR, the iron corrective was reduced. This increased the AR.
Clinker ball formation occurred on several occasions and caused clinker cooler stoppages
Clinker ball formation coincided with peak-periods of liquid phase content and of high AR.
The phenomena disappeared when AR and SR could be brought back to initial levels.
Clinker Balls: Plant Example

## Slide 61
61
Periods of clinker ball formation
Variations due to unsteady supply of AR
Alumina ratio
Silica ratio
Liquid phase
Clinker Balls: Plant Example

## Slide 62: Clinker Microscopy: A Diagnostic Tool

## Slide 63
63
Clinker phases
Microstructure
distribution
homo- geneity
porosity
content
Evaluation of
Clinker quality
(e.g. grindability, soundness, setting behavior, “strength development”)
Process conditions
(e.g. raw meal properties, burning and
cooling conditions)
size
morpho- logy
Microscopy provides information which is not available from routine measurements

## Slide 64
64
Belite and free lime clusters due to oversized quartz and limestone grains => ineffective raw meal grinding.
Example: Impact of raw meal preparation

## Slide 65
65
Small sized interstitial mass and no alite decomposition are characteristic for effective clinker cooling.
Example: Investigations of cooling conditions

## Slide 66
66
Example: Impact of reducing conditions
Practical, simple test for reducing conditions: “Magotteaux Test”
Microscopy can show effects of reducing conditions, e.g. decomposition of alite starting from edge of pores (access of gas)

## Slide 67
67
Microscopy: Impact of P2O5
4.2% P2O5 in belite

## Slide 68
68
Microscopy can be supported by SEM measurements
Spotanalysis of belite in direct contact with free lime

## Slide 69: Conclusions

## Slide 70
70
Investigate and exploit the potential for raw mix and clinker optimization with regard to
  Improve the burning behavior
  Improve product quality
  Reduce materials cost
    Consider the use of alternative materials in this context
Make use of powerful diagnostic and prognostic tools to assess the potential of optimization possibilities
Conclusions