## Slide 1: Product Optimization
PPE Course

## Slide 2
2
Understand the relevance of product optimization
Know the systematic approach for product optimization
Have an overview on the different factors influencing cement performance
To familiarize with adequate control parameters
Objectives

## Slide 3: Agenda
Basic Aspects for Product Optimization
4
The Product Optimization Decision tree
11
Clinker Quality
13
Set Regulator
28
Mineral Components
48
Cement Grinding
60
Cement Additives
75
Conclusions
84

## Slide 4: Basic Aspects for Product Optimization

## Slide 5
5
Optimization of the final product contributes to cost reduction, customer satisfaction and sustainable performance
Better cost management
  Reduction of production costs
  Increase of production capacity
  Lower or delayed need for investments
Compliance with market requirements
  Improvement of product quality
  Product differentiation
Sustainable ecological performance
  Reduction of CO2-output
  Extension of raw material resources

## Slide 6
6
An important indicator for product optimization is the reduction of the clinker factor
Information from the CO2 inventories of the group

## Slide 7
7
Clinker factor development in Germany (Source VDZ), based on an extrapolated product portfolio
Stable slag availability, trend to higher fineness, replacement of CEM I by CEM II
Reduced slag availability (-25%), thus reduced CEM II-S production

## Slide 8
8
The reduction of the clinker factor allows to decrease significantly the specific CO2 emissions per ton of cement
To reduce the clinker factor is the most effective measure and represents the highest potential for CO2 reduction

## Slide 9
9
There are several threats for the further reduction of the clinker factor in the Group
Level | Threats
Business Plan, Budget | MIC availability / costs Direct use of MIC by customers Prescriptive instead of perform oriented standards Market tendency to high early strength cements
Marketing (“daily operation”) | Quality race amongst competitors Missing experience / acceptance for CC
Manufacturing (“daily operation”) | Low early strength of composite cements Lower clinker quality / uniformity due to use of AFR Resistance to clinker mineralization Technical constraints

## Slide 10
10
Pre-requisite for the product optimization is a clear definition of the product portfolio and quality requirements
  Market requirements /strategy
  Cement standards
  Availability of MIC’s
  Raw material situation
  Production facilities
Definition of Product Mix and
Product Quality Requirements
  Performance improvement of intermediate and final products
  Process optimization
  Optimal cement design
Achievement of Product Requirements
at Minimum Operation Cost
Task:
Product Optimization
Responsibility:
Production
Task:
Product Mix Definition Responsibility:
Marketing &
Production

## Slide 11: The Product Optimization Decision tree

## Slide 12
12
Systematic approach for product optimization

## Slide 13: Clinker Quality

## Slide 14: The Product handbook can be found on Google Drive

## Slide 15
15
C3S, C3A, alkalis and sulfur determine to a great extent the strength potential of the clinker
* mineralized clinker

## Slide 16
16
Influence of clinker minerals on cement properties
Clinker phase | Name | Typical Content (%) | Early strength | Final strength | Setting time | Water demand | Sound-ness
C3S | Alite | 60 – 70 | ä | ä | - | - | -
C2S | Belite | 10 – 20 | æ | ä | - | - | -
C3A | Aluminate | 7 – 10 | ä | æ | æ | ä | -
C4AF | Ferrite | 7 – 10 | (æ) | (ä) | - | (æ) | -
CaO free | Free lime | 0.5 – 1.5 | ä | - | æ | - | æ
MgO | Periclase | 0.6 – 1.2 | - | - | - | - | æ
Alkali sulphates |  | 0.6 – 1.2 | ä | æ | - | ä | -
ä increase æ decrease - no effect

## Slide 17
17
Result of HTEC reactivity testing: C3S is main driver for the strength development at all ages
Good range of C3S

## Slide 18
18
42% of Holcim clinkers are undersaturated in sulfur
ATR 2014
Chart: SO3 [%]
line | 0 | 1.94
Sulfur excess
Alkali excess
molar A/S = 1
In 2010 65% of the clinkers of the Group were under-saturated in sulfur

## Slide 19: Example: Alkali sulfates and strength potential

## Slide 20
20
Other minor elements can impact the clinker properties
ä increase æ decrease - no effect
*On clinker basis; level may vary with specific plant conditions and requirements
Belite stabilization
Increased Ferrite

## Slide 21
21
Comments on some specific elements:
  Cr: Effect on health & safety of the final product (chromate eczema) if present as Cr (VI)
  Zn: Set retardation and low early strength at concentrations of 0.5% in clinker (not relevant for practice)
  V: Possible increase due to use of special Petcoke quality, concentrations, however, still too low for relevant effect.
For further reference regarding typical heavy metal contents, consult the Memo 07-14135-Trace Elements on Google Drive.
Heavy metals have in general not a significant impact on clinker quality

## Slide 22
22
Besides the chemical composition, certain process measures have be followed to ensure good clinker quality
Maximize / Optimize:
Raw meal homogeneity
Raw meal fineness
Coarse fuels (AFR!)
Raw Material Prep.
and Grinding
Avoid:
Overheating
Lazy long flame (flat temp. profile)
Sulfur cycles
Clinker dust formation
“Reducing” conditions
Slow clinker cooling
Clinker Burning
and Cooling

## Slide 23
23
Fineness:
  The smaller the particles and the closer they are, the smaller the diffusion distances. With excessive particle size or distance between two reactants, the reactions cannot take place within a reasonable time.
Homogeneity:
  Insufficient raw meal homogeneity can cause an oversaturation of carbonate or siliceous particles in certain areas.
  If there is a lack of limestone components and a concentration of siliceous components, a cluster of belite occurs.
  If in contrary there is a surplus of carbonate component, the CaO which has not reacted remains as free lime clusters.
Influence of raw meal preparation

## Slide 24
24
Proper raw meal preparation is crucial to achieve a fine and homogeneous clinker microstructure and a good reactivity
Good: Fine & homogenous clinker microstructure (adequate raw meal fineness & uniformity)
Bad: Coarse & heterogeneous microstructure (raw meal too coarse and not uniform)
Legend: Alite is brown, belite is blue.

## Slide 25
25
Influence of burning conditions on clinker quality

## Slide 26
26
Process and quality control of AFR and of kiln operation is crucial to ensure the reactivity of the produced clinker
1 day strength development CEM I 52,5R
Example Höver: Increase of TSR went along with reduction of early strength
Use of AFR poses more risks for process problems in the kiln due to their less favorable characteristics regarding ease of combustion.
Critical aspects to be controlled are the "ash” integration from AFR, reducing conditions and inadequate temperatures profiles in the kiln.

## Slide 27
27
Systematic approach for product optimization

## Slide 28: Set Regulator

## Slide 29
29
The set regulator plays an essential role regarding cement performance
Type (Gypsum / Anhydrite) and dosage of calcium sulfate has an effect on:
  Setting behavior
  Strength development
  Flowability / storage stability
Use of industrial gypsum implies advantages and disadvantages:
  lower cost
  high moisture leads to handling problems and requires sufficient drying capacity of the mill system
  possible presence of minor elements prolonging setting times and reducing strength

## Slide 30
30
Industrial gypsum is widely used within the Holcim Group
Source: ATR 2009

## Slide 31
31
Industrial gypsum sources
Type | Source | Impurities
Desulfogypsum | Flue gas desulphurisation | SO32-, Cl
Phosphogypsum | Fertilizer and phosphoric acid production | P2O5, F
Fluorogypsum | Hydrofluoric acid production | CaF2
Borogypsum | Boric acid production | B(OH)3
Titanogypsum | TiO2 production | TiO2, Fe(SO)4
Organogypsum | Citric, formic and tartaric acid production | Organic compounds

## Slide 32
32
Regular set
  proper balance between clinker (C3A) reactivity and soluble sulfate
  formation of needle-like ettringite
False set
  excess sulfur compared to (C3A) reactivity
  formation of secondary gypsum
  can be overcome by re-mixing
Flash set
  lack of sulfur compared to (C3A) reactivity
  formation of angular monosulfates
  most critical case, not reversible!
The setting behavior is related to the balance between soluble sulfate and C3A reactivity

## Slide 33
33
Illustration of setting types
33

## Slide 34
34
Gypsum (dihydrate) and anhydrite are the natural calcium sulfates that can be used as set regulator in the cement
Designation | Formula | Range of Stability °C | Solubility at 20°C | Occurrence in Nature | Occurrence in Cement
Dihydrate | CaSO4 .2H2O | >40 | 0.2 | Yes | Yes
Hemihydrate | CaSO4 .½H2O | Metastable (110°-180°C) | 0.95 | No | Yes
Anhydrite III | CaSO4 | Metastable (120°-250°C) | 0.95 | No | Yes
Anhydrite II (nat. Anhydr.) | CaSO4 | 40-1180 | 0.2 | Yes | Yes
Anhydrite I | CaSO4 | >1180 | --- | No | (~clinker)

## Slide 35
35
During cement grinding, the gypsum gets dehydrated and new types of sulfate phases are formed
At normal grinding temperatures at least a part of the gypsum gets dehydrated to hemihydrate, anhydrite III formation is rather scarce.
The degree of dehydration depends on the temperature, residence time, and humidity in the mill.
At high product temperatures (> 85 °C) the same reactions can occur in the silo (risk of lump formation).
1) CaSO4 · 2 H2O  CaSO4 · 0.5 H2O + 1.5 H2O
2) CaSO4 · 0.5 H2O  CaSO4
Gypsum
Hemihydrate
Hemihydrate
Anhydrite III

## Slide 36
36
Hemihydrate and anhydrite III have a higher solubility compared to gypsum and natural anhydrite
Temperature [°C]
Solved CaSO4 [%]
hemi-hydrate
gypsum
nat. anhydrite
Anhydrite III

## Slide 37
37
Increase addition of set regulator
  Set point maximum standard SO3
  Stop addition of set regulator to mill
Take samples every 5 to 10 min over 30 to 60 min (frequency and duration depends on mill type/system)
  Sample quantity according to scope of testing (5-20 kg)
Test samples with different SO3 content for selected properties
  at least: setting times, mortar compressive strength
  ideal concrete: workability, compressive strength
The optimum gypsum content in the cement has to be determined on industrial scale
Notes: Min 5-6 samples are required to conclude on optimized SO3
Do not do the test when the Silo is empty!!

## Slide 38
38
Industrial SO3 optimization should be done:
  for each cement type
  for each mill system
  after significant changes of
    clinker composition (i.e. C3A content, A/S ratio)
    cement composition (e.g. increase of MIC content)
    process temperatures (e.g. improvement of mill ventilation)
The optimum gypsum content in the cement has to be determined on industrial scale

## Slide 39
The dosage of the set regulator has a strong influence on strength development (example pozzolana cement)

## Slide 40
40
At high cement temperatures, gypsum can dewater in the silo leading to problems with lump formation
Lump formation can be caused by:
  High product temperatures at silo entrance and subsequent gypsum dehydration
  Leakages in the silo walls
  Excessive water injection into the mill
Solid blocks
Soft lumps in cement

## Slide 41
41
Water entering the silo
  Leakages
  Gypsum
  Moisture of water injection
“Bridging” phases are formed
  Ettringite
  Syngenite
Consequence
  Loss of flowability
  Lump/build up formation
  Pre-hydration (retardation, strength loss)
Principle of lump formation
CaSO4 x 0.5 H2O + 1.5 H2O
CaSO4 x 2 H2O
> 80 °C
Side of coating formation
Product Optimization, CM-MMT, LAF, 2014-10-28

## Slide 42
42
Keep cement temperature below 75/80°C in order to avoid dehydration of gypsum
  Avoid grinding of hot clinker
  Optimize air ventilation
  Inject water into one or both grinding chambers
  Install cement cooler
Reduce water input via gypsum
  Partial or complete substitution of gypsum by anhydrite
  Optimize gypsum for each cement type (avoid overdosing)
Avoid water penetration
  Control silo roof, walls
  Adequate silo ventilation
Reduce storage time
  Empty silos regularly
Measures to avoid lump formation
Notes: Most of the time, Gypsum is cheaper

## Slide 43
43
Adjust clinker properties
  Balance alkali sulfur ratio (no high reactive C3A)
  Reduce K2O content (avoid syngenite formation)
  Adjust adequate free lime (“water absorbant”)
Improve cement flowability
  Use cement additives to improve flowability
  Adjust cement fineness (flowability improves with higher fineness)
Measures to avoid lump formation (cont.)
Notes: Adjust adequate free lime (in case CaOf level is low)

## Slide 44
44
Take samples at mill outlet and silo inlet; silo outlet samples shall be taken during dispatch
Take temperature of cement at mill exit and silo inlet
Investigate moisture content in the samples by differentiating
  Inherent moisture
  Gypsum/Hemihydrate water
  Syngenite
  Portlandite/C-S-H water
A sampling campaign helps to understand the origin of the lump formation problem

## Slide 45
45
Staggered LOI
  Easy and cheap
  Gypsum and hemihydrate cannot be distinguished
  In the end sample should be heated up to 950 °C to get complete LOI (plausibility check)
Methods to determine the dehydration degree and reasons for lump formation
Temperature range | Type of moisture
20 – 70 °C | inherent moisture (water spray, water ingress)
70 – 250 °C | gypsum, hemihydrate crystal water
250 – 600 °C | Syngenite, portlandite crystal water

## Slide 46: Methods to determine the dehydration degree and reasons for lump formation
Thermal analysis - (Thermal Gravimetric Analysis)/ (Differential Scanning Calometry)
  Differentiation between gypsum and hemihydrate (anhydrite to be calculated)
  Identification of hydration products (Portlandite, ettringite) and typical bridge forming minerals (syngenite)
  Equipment not available in most plants
XRD
  Differentiation of gypsum, hemihydrate, anhydrite
  Identification of hydration products and typical bridge forming minerals (syngenite)

## Slide 47
47
Systematic approach for product optimization

## Slide 48: Mineral Components

## Slide 49
49
Reduction of clinker factor
Improved late strength
Improved durability
  Frost resistance
  Higher resistance against acid attack
  Lower risk of alkali silica reaction
Improved workability
  Lower water demand
Better grindability
The use of Mineral Components (MIC) can have several positive effects…

## Slide 50
50
…but due to the lower clinker factor composite cements suffer from a low early strength.
0
10
20
30
40
50
60
Strength [MPa]
0
10
20
30
40
50
60
Grinding energy [kWh/t]
2 d
27.1
16.8
16.9
12.0
19.4
28 d
48.9
36.5
37.7
41.8
45.8
Energy
46.7
33.4
33.0
39.5
43.4
Blaine
3825
4110
3977
3704
3785
OPC
Limestone
Pozzolan
Fly ash
Gbfs
MIC content: 21 - 35 %
Source: ATR 2001

## Slide 51
51
The typical MIC dosages depend on the cement application and standard limits.
 | General purpose | Sulfate resistance | Low heat of hydration | Chemical resistance*
 | Weight % |  |  | 
Blast furnace slag | 25 – 40 | 70 | 50 | 60
Fly ash (class F) | 15 – 30 | 30 | 30 | 40
Natural pozzolans | 15 – 30 | 30 | 30 | 40
Limestone | 10 - 25 | n.a. | n.a. | n.a.
* Provided that the w/c-ratio of concrete is reasonably low
Notes: Chemical resistance for higher acid concentration (ex: agricultural building)

## Slide 52
52
Mineral components can be classified by their reaction mechanism
BFS
OPC
Meta-kaoline
Silica fume
CaO
SiO2
AI2O3
Natural pozzolan
ClassF fly ash
Lime- stone
Inert
Pozzolanic
Latent hydraulic
Hydraulic
Increasing Reacitivity
Class C
Fly Ash

## Slide 53
53
Limestone
  Usage of good quality limestone without clay and organic contamination
Natural pozzolan
  Selective mining according to pozzolanic activity
  Pre-homogenization
Granulated blast furnace slag (GBFS)
  Optimization of slag quality at blast furnace or granulator (e.g. Al2O3-content, basicity, glass content)
Fly ash
  Selection of fine fly ash from filter of power station
  Beneficiation (extraction of un-burnt, coarse particles)
The optimization of MIC is often not in the hands of the cement plant

## Slide 54
54
Characterization of natural pozzolan
Parameter | Reverences / limits
Relevant standards | EN 197-1 ASTM C311
Chemical composition | 
Desirable: SiO2 + Al2O3 + Fe2O3 | >70%
Mineralogical composition | 
Desirable: glass, zeolite Critical: clay (water demand) | > 50%; > 20%* < 10%
Hydraulic activity | 
Strength activity index Pozzolanicity test (Ca(OH)2) Pozzotech WP13 | >75% EN 196-5

## Slide 55
55
Example: Upgrading pozzolan quality at Nobsa
1st step: Selective Mining based on Pozzolanic Activity
2nd step: Pre-blending of Pozzolan
Result:
Source: Jairo Hernandez, Cem.Boyacá

## Slide 56
56
Relevant GBFS parameters
Parameter | References/ limits
Relevant standards | EN 197-1 ASTM 989
Chemical composition | 
Desirable: CaO,MgO, SiO2 Basicity, e.g.(C + M)/S Critical: SO3, S2- TiO2 Heavy metals | min. 2/3 min. 1.0 < 4.0 %, < 2.5 % Ideal < 0.5%
Mineralogical composition | 
Glass content | min. 2/3 (ideal > 90%)
Hydraulic activity | 
Strength activity index | ASTM C 989

## Slide 57
57
Characterization of fly ash
Quality characteristics | References and limits
Relevant standards | EN 197-1 ASTM C618
Chemical composition | 
Desirable: SiO2, Al2O3,(CaO), Fe2O3 Critical: SO3, Carbon (LoI) | max. 5%
Mineralogical composition | 
Desirable: glass Critical: CaO free | > 25% (typical 50-80%) < 1% EN 197
Hydraulic activity | 
Activity index Pozzolanicity test (Ca(OH)2) | ASTM C 311 EN 196-5
Granulometry | 
Spherical particles Fineness | 

## Slide 58
58
Kiln dust that cannot be recycled in the kiln system should be added to the cement (when allowed by the standards)
  Bypass dust
  Dust of long kilns and Lepol kilns
It is recommended to use filter dust collected during direct operation in the cement to reduce cycles of highly volatile elements (Hg, Tl, Cd, Cl)
Use of kiln dust in the cement
Element | Average | Maximum
K2O | 10.5 | 25.0
Na2O | 2.5 | 4.1
SO3 | 8.7 | 16.5
Cl | 5.5 | 9.5
Bypass dust usually contains high concentrations of alkalis and sulfur
  can increase early strength
Limiting factor is usually the limit (Cl < 0.1 %) in cement
Handling and dosing are critical, due to stickiness of the material

## Slide 59
59
Systematic approach for product optimization

## Slide 60: Cement Grinding

## Slide 61
61
Besides the properties/proportioning of components, the grinding process has a strong influence on cement quality
Fineness / particle size distribution (PSD)
  Water demand and setting behavior
  Strength development
Grinding temperature / residence time (dehydration of gypsum)
  Setting behavior
  Flowability / storage stability
Trends with modern grinding systems (e.g. vertical mills)
  Narrower particle size distribution
  Lower grinding temperatures and residence time (less dehydration of gypsum and lower contents of easily soluble sulphates)

## Slide 62
62
Water demand to achieve a certain flow depends on:
  Reactivity of cement constituents (clinker)
  Water demand of cement constituents (e.g. pozzolan, silica fume)
  Cement fineness (finer -> higher water demand)
  PSD of cement (narrower -> higher water demand
  Concrete composition (cement content, aggregate composition…)
High water demand has a negative influence on strength

## Slide 63
63
Workability: Water is required to fill the voids among the cement particles
characteristic diameter x’
fines
Water needed for early hydration products
Water needed to fill void volume
Water demand

## Slide 64
64
Ideal clinker PSD to achieve maximum reactivity
  High fraction < 30 mm
  High fineness
  Narrow PSD. For the resulting cement, however, a wide PSD is better (workability)
Strength development is determined by the reactivity and fineness of the cement constituents
Particle size (mm) | Main influence on:
0 – 3/10 | 1d strength
3/10 – 25 | 28d strength
25 – 50 | 90d strength
Ideal for high strength
Clinker fineness:
μm
%
30 μm
3 μm
not ideal

## Slide 65
65
In compound grinding the cement components are distributed according to their grindabilities
Broad PSD of cement
MIC concentrated in fine fraction
Clinker in coarse fraction
Narrow PSD of cement (high water demand)
Similar PSD of clinker and MIC
Soft MIC (e.g limestone, pozzolan)
Hard MIC (e.g. GBFS)
μm
%
MIC
Clinker
μm
%
MIC
Clinker

## Slide 66
66
The following measures can be applied to improve cement fineness and particle size distribution
Optimization of tube mill performance
  Adjustment of ball charge
  Adjustment of material level in the first chamber
  Adjustment of the circulation load
Use of modern grinding technologies (high efficiency separator, semi-finish grinding, vertical mill)
Separate grinding of clinker and MICs

## Slide 67
67
Separate grinding of clinker and MIC gives more flexibility for the optimization of the particle size distribution
Compound grinding
Separate grinding
soft
hard
Materials with different grindabilities: Effects on the product particle size distribution

## Slide 68
Potential for CF reduction through separate grinding of clinker and MIC typically in the order of 5%
Best case examples for CF reduction with separate grinding
Application of separate grinding is limited to plants with certain flexibility in production facilities
68
Separate grinding can give significant potential for CF reduction depending on the specific plant situation
Plant | Cement Type | CF Reduction (%)
Barroso | Slag cement | 16
Cantagalo | Slag cement | 13
Cartago | Pozzolanic cement | 10

## Slide 69
69
For composite cements, the fineness control is to be based on sieve residues (and not on Blaine)!!
Soft MIC (e.g limestone, pozzolan)
The residue in composite cements is in general clinker
For blended cements:
  Always control fineness on basis of sieve residue!
  In particular when using soft MIC
Blaine
  Mainly influenced by very fine particles
  Increase of MIC proportion can increase Blaine significantly

## Slide 70
70
Information which is directly accessible:
  Residues [%], like R15, R20, R32, R63.3, etc. almost continuous.
  Position parameters [mm], like d10, d50, d90
Laser granulometry helps to get a clearer picture of the cement psd
Density distribution q3
Cumulative distribution, Q3
d50
100-R5
Note: We get a Volume distribution!

## Slide 71
71
The RRSB distribution is given by a mathematical function, described by two parameters:
  The position parameter d’ (or x’)
  The slope or steepness parameter n
Experience has shows that it (often) fits quite nicely to particle size distributions produced by comminution processes.
Double logarithm yields the function of a line, which can be plotted in the RRSB diagram.
Practical interpretation:
  d’: position parameter [mm] with 63.2% passing
  n: slope of the line in the RRSB diagram. The higher the slope the narrower the distribution.
Evaluation of the RRSB parameter

## Slide 72
72
There are different methods of evaluation
Typically the lowest and the highest 10% of the distribution are not considered
RRSB Diagram
n = 0.74
x
‘
= 19.6
µ
m
1
2
3
4
6
8
12
16
24
32
64
48
96
128
200
1.5
99.9
99
95
90
80
63.2
50
40
30
20
10
5
4
3
2
1
n = 0.74
x
‘
= 19.6
µ
m
1
2
3
4
6
8
12
16
24
32
64
48
96
128
200
1.5
99.9
99
95
90
80
63.2
50
40
30
20
10
5
4
3
2
1
Particle size [um]
Passing [%]
Slope
Char. Diameter

## Slide 73
73
The n parameter is a often function of the grinding system and the cement constituents
Chart: BM-HRM-VRM max
n (HRM) > n (VRM) > n(BM)

## Slide 74
74
Systematic approach for product optimization

## Slide 75: Cement Additives

## Slide 76
76
Cement additives are used for the purpose of process and product optimization and for the production of special cements
Type of Additives | Cost / Dosage* | Purpose
Grinding aids (Process improvement related) | 0.1-0.4 USD/t 100 – 500 g/t | Reduction of specific energy consumption Improvement of mill output Reduction of pack set (better flowability)
Quality improvers (Product properties related) | 0.5 – 1.0 USD/t 300 – 5000 g/t | Grinding aid and strength enhancer Clinker factor reduction Water reduction
Others (Particular properties related) | Up to 5000 g/t Up to 500 g/t Up to 2000 g/t Up to 2000 g/t | Cr(VI) reduction Air entrainment Retardation Water retention
* indications per t of cement

## Slide 77
77
Additives reduce the inter-particle forces
  Reduced coating of grinding balls and mill internals
  Better dispersion of particles in separator feed
  Reduction of mill filling level (decrease of residence time)
  Improved flowability of cement
Additives reduce the trend of the ground particles to agglomerate
Agglomeration
Dis-Agglomeration
Source: Grace
Coating
Clean grinding balls

## Slide 78
78
Depending on the type of product, a variety of cement additives can be applied during cement grinding
Cement type | Grinding aids | Quality improvers |  |  | Others | 
 |  | Strength enhancer | Water reduction | Set control | Air entrainer | Water retention
OPC | typical | possible |  |  |  | 
OPC white | typical |  |  | possible |  | 
Limestone cement | typical | typical |  |  |  | 
Masonry cement |  |  |  | possible | possible | typical
Fly ash / pozzolan cement | possible | possible | possible |  | possible | 
Blast furnace slag cement | possible | typical |  |  |  | 
Cement for self compacting concrete | possible |  | typical | possible |  | typical
Note: Cr[VI] reducers can be applied for all cement types depending on the requirements

## Slide 79
79
Trials with cement additives are particularly indicated under the following circumstances
Grinding aids (typical potential: 5 - 10% higher mill output or lower electrical energy)
  Bottlenecks in cement grinding capacity, unfavorable electricity tariffs.
  High specific electrical energy consumption during cement grinding (e.g. > 45 kWh/t).
  “Pack set” problem, problems with cement handling.
Quality improvers (typical potential: 2 - 3% reduction in clinker factor)
  Opportunity for further clinker factor reduction (increase of cement volumes, cost and CO2 reduction).
  Cement setting or strength development problems.
Others:
  Production of special cements/binders with better margins (masonry cement, road binder, …).

## Slide 80
80
In order to get comparable data, a procedure for plant trials was established consisting of different steps
Laboratory testing of additives
Pre-selection of additives for the trials
Benchmarking of different additives
Testing best additive
Proving suitability of additive Final evaluation
Constant fineness
Constant composition
Variation of additive dosage and type
Variation of:
Cement composition
Cement fineness
Additive dosage
Slow adjustment of:
fineness
composition
if necessary to keep quality
Selection of best suited additive
Optimization of quality/ production rate
Validation of results
Evaluation of potential downstream impacts
Step 1: Short term trials 6 - 8 h each
Step 2: Short term trials 6 - 8 h each
Step 3: Long term trial ideally 1 month
Step 4: Check of additive effectiveness
Periodic short term trials (e.g. every 6 month)
Industrial trials
Preparation

## Slide 81
81
Content
  Market assessment
  Additive testing on industrial scale
    Planning
    Execution
    Mill operation
    Downstream impacts
  Additive effect and control
    Standard requirements
    Chemical ingredients and their effects
    Lab testing of new additives
    Quality control in routine application
  Commercial viability of test results
Best practices for the use of cement additives have been recently summarized in a handbook.
Can be found on Google Drive

## Slide 82
82
E. R. = Reduction in spec. energy demand at 4000 cm2/ g (Blaine)
Without GA
Amine based
Glycol based
0.50 mm
Screen Grid Width
0.25 mm
9%
29%
19%
46%
9%
31%
E. R.
0%
12%
11%
Grinding Aid
Flowability of the cement with additives can be determined by a simple test using a sieve and a shock table.
Tools needed:
Sieve & Shock Table
Further references:
PCA Info: http://www.cement.org/manufacture/man_packset.asp
ASTM C1565-04 Standard Test Method for Determination of Pack-Set Index of Portland Cement
Test result:
Passing of cement through sieve

## Slide 83
83
EU directive requires a limit of 2 ppm soluble CrVI in order to reduce the risk of chromium eczema
  CrVI is formed during clinker burning
  Composite cements have generally lower CrVI concentrations (dilution)
  Usually the CrVI content is higher than 2 ppm
Typical reducing agents
  Iron sulfates (hepta/tetra/mono hydrate)
  Tin sulfates
  Typical costs between 0.5 – 1.0 €/t
Optimum dosing point depends on type of agent
Chromium reduction – why and where?

## Slide 84: Conclusions

## Slide 85
85
Conclusions
Continuous and systematic Product Optimization is a key measure to achieve cost and market leadership and to fulfill CO2 targets.
Product Optimization can not just be left to the quality assurance department, it requires combined effort of the plant and line management.
Cement plant must ensure effective communication and cooperation with marketing and sales
  to be aware of market requirements
  to bring forward producers’ interests
  to assure optimal product mix and quality targets

## Slide 86
86
Optimization of clinker quality comes always first (clinker is finally the most essential ingredient in the cement and it is under our control).
Actions for optimization are to be carried out step by step, in order have a clear picture on the effects (do not change several parameters at once).
A sufficient duration of the optimization tests is to be ensured, in order to obtain representative results.
All the realized tests have to be properly documented (incl. process data) for further reference.
General messages for product optimization