## Slide 1: SO2 Emission Control & Reduction
Technical Development Program for Process Performance Engineers – SPREAD 2016
Mirko Weber

## Slide 2
2
Correct, Pyrite – FeS2

## Slide 3
3
Environmental impact of SO2
How to analyze/solve a SO2 emission problem
Formation of SO2 in kiln system
Primary measures
Secondary measures
Content

## Slide 4
4
Smog killed 8’000 people in London in 1952
SO2 contributes to smog and acid rain formation
Smog in large cities nowadays
Acid rain damages vegetation
Inversion situation

## Slide 5
5
Smog killed 8’000 people in London in 1952
Inversion situation
SO2 contributes to smog and acid rain formation

## Slide 6
6
Steam plume
Secondary plume
SO2 can lead to Opacity – Detached plume

## Slide 7
7
Standard reporting in mg/Nm3 dry @ 10% O2
Transformation of SO2 units
SO2 Emissions expressed in mg/Nm3 wet*
* Wet according to measurement principle (in situ, hot extractive, etc) ** Water content of gas (vol %)
SO2 Emissions expressed in mg/Nm3 dry
SO2 Emissions expressed in mg/Nm3 dry @ y % O2
SO2 measurement (in ppm)
?
Conversion: ppm x 2.86 = mg/Nm3
Wet – dry conversion:
O2 correction:

## Slide 8
8
General procedure for emission abatement
Elimination of precursors
Primary measures
Secondary measures

## Slide 9
9
Fuel
  Coal: 0.5 - 4.0 % S
  Fuel oil: 1.0 - 2.5 % S
  Petcoke: 3.0 - 8.0 % S
  Tires: 0.8 - 4.0 % S
Raw material:
  Variable from < 0.1 % to > 1 % S as SO3
  SO3 average : ~ 0.45 % SO3
Sulphur input into the kiln system via fuel and raw materials vary

## Slide 10
10
Sulphured organic compounds
Pyrite (FeS2)
Sulfides (CaS)
Sulphites (CaSO3)
Sulphates (CaSO4)
Sulphur input into the kiln system - Compounds in raw material have different volatilities
High volatility
Low volatility

## Slide 11
11
Pyrite - Raw material
30 – 80 % forms SO2
S-Fuel (AF or trad.)
100 % forms SO2
„100 % SO2-Barrier“
SO2 + CaO + ½ O2  CaSO4
Sulphate from raw material
30- 80 % forms SO2
Raw mill
30 – 60 %
SO2 absorption in compound operation
SO2 emissions of preheater kilns are basically fuel independent – exception: SO2 from bypass
Filter
10-30 % SO2 Absorption

## Slide 12
12
Empirical SO2 capture in PH tower (%)
PH exit gas temperature (°C)
370
70% capture > 30% “emission”
SO2 emissions from pyrite depend on temperature
Expected pyritic sulfur contribution to SO2 emissions can be verified
  Analysis of all raw meal components
  Expulsion test
  Theoretical calculation For dry SP kilns e.g. at 370°C, assume 30% of pyrite goes to the emissions in direct operation, ca. 15% in compound operation

## Slide 13
13
Primary Measure for preheater kilns: Increase mill running time > up to 50% less SO2 emissions
SO2 absorption in mill and filter - example with high retention rate
SO2 emissions lower in compound mode

## Slide 14
14
quench
chamber
clinker
discharge to cement
bag filter
bypass
bag filter
Main kiln gas SO2 1’000 mg/Nm3
Bypass gas SO2 15’000 mg/Nm3
Kiln inlet gas SO2 32’000 mg/Nm3
Main stack SO2 1’400 mg/Nm3
Example shows a 5% bypass increasing SO2 emissions by 40% at the main stack

## Slide 15
15
*SOx = SO2 + SO3
S-Fuel
100 % forms SOx*
Pyrite - Raw material
30 – 50 % forms SO2
Kiln dust
40-60 % SO2 Absorption
Filter dust
10-30 % SO2 Absorption
Sulphate - Raw material
30- 80 % forms SO2
Sulfur from fuel and raw material contributes to SO2 emissions in long kilns (wet or dry)

## Slide 16
16
Dry preheater kilns
  Selective quarrying if possible, reduce high volatile S input
  Increase mill running time
  Recycle bypass gas to cooler (references in legacy Lafarge plants)
Wet/dry long kilns
  Reduce S-input via fuels or raw material
  Homogenize fuels (in case of SO2 peaks)
  Reduce sulfur volatility
    Avoid combustion in reducing conditions , provide excess air (no CO!)
    Avoid temperature peaks and over-burning (CaOf 0.8-1.5%)
    Avoid long flame, adjust burner momentum (see example)
    Assure sulfatization of the alkalis
    Burner position parallel to kiln axis
    Optimum fuel fineness and dispersion
    Stable kiln operation (Kiln Master)
    Improve burnability of kiln feed by e.g. reducing the SM
SO2 elimination of precursors & primary measures – optimize combustion in case of long kilns

## Slide 17
17
SO2 at stack in function of kiln O2 (wet kiln line)
Sulphur volatility depends on the oxygen concentration in the kiln (wet/long kilns)
Chart: O2 at kiln inlet [%]
| 0.9 | 1.5 | 2 | 2.5 | 3 | 4
 | 800 | 550 | 500 | 340 | 260 | 190

## Slide 18
18
Dry methods
  Addition of Ca(OH)2, Na2CO3, activated coal, spongiacal lime (high specific surface)
  Polvitec (activated coke filter)
Semi-dry, Semi-wet methods
  Injection of hydrated lime slurry (into the conditioning tower)
Wet technologies
  Wet scrubber
Secondary measures – from dry to wet technology

## Slide 19
19
Efficiency of dry Ca(OH)2 is influenced by temperature
Needs 350°C and more
Addition of dry lime for SO2 abatement
Gas phase reaction
(dry)
Aqueous
phase
(wet)

## Slide 20
20
Addition of dry lime for SO2 abatement, Höver (Germany)
Tests with addition in front of filter or in conditioning tower showed low efficiency
Best practice: addition of dry lime to the kiln feed
Dosing via rotary valves
Jet transport of lime to bottom of bucket elevator
Approx. 950 kg/h lime
Control of addition in function of SO2 at stack
Reduction from max 1’300 to below 400 mg/Nm3 (kiln prod: 2’600 t/d)

## Slide 21
21
Investment 30 Mio CHF
Reduction from max.1’500 to 7 mg/Nm3
Activated coke: 2’600 tpy
Costs 400 CHF/t coke
Eliminates as well NH3, VOC, Hg, etc.
Operating costs ca. 5 CHF/tcli (1.5 CHF/t cli for coke)
Activated coke filter “Polvitec” in Siggenthal (Switzerland)

## Slide 22
22
Injection of “micromist” into the cooling tower
Gas phase reaction
(dry)
Aqueous
phase
(wet)

## Slide 23
23
Example:
Gas flow 350’000 Nm3/h
Guarantee: 90% SO2 reduction, 94% HCl reduction
Investment costs approx. 1- 1.5 Mio USD
High operating costs in case of permanent operation (lime costs 93 USD/t)
Sulfur goes back to kiln (circulation phenomena)
Injection of “micromist” into the cooling tower, example

## Slide 24
24
Mixer
Raw gas with SO2
Inlet with quench
Absorber sump
Mist separator
Clean gas
Stack
Contact zone between SO2 and CaCO3
Treatment and dewatering of gypsum suspension
Recircul. pumps
CaCO3 + SO2 + 2 H2O + ½ O2  CaSO4 x 2 H2O + CO2
Wet limestone scrubber technology is the ultimate measure
CaCO3 + SO2 + 2 H2O + ½ O2  CaSO4 x 2 H2O + CO2

## Slide 25
25
Wet limestone scrubber technology
Mixer
Raw gas with SO2
Inlet with quench
Absorber sump
Mist eliminators
Clean gas
Stack
Contact zone between SO2 and CaCO3
Treatment and dewatering of gypsum suspension
Recircul. pumps

## Slide 26
26
Wet scrubbers in Legacy Holcim
Untervaz, CH
Midlothian, US
Portland, US

## Slide 27
27
Gypsum for finish products is produced by scrubber system
Gypsum conditioning
Gypsum dosage
Flocculant
Reagents conditioning
Scrubber
Lime- stone & Dust
H2O
air
Kiln gas
H2O
old / new stack
H2O
H2O
Absorber tower incl.
  Redundant gas quench at the scrubber inlet
  3 nozzle stages
  Mist eliminator (chevron type 3 layers)
Stack (fixed to the preheater tower)
Pumps for circulating the slurry (e.g. 3)
Gypsum dewatering (hydrocyclone, settling tank, centrifuge and weighing belt. Flocculant generally not required)
Silos for reagent
Emergency tank (for emptying scrubber or buffering gypsum slurry) (e.g. 150 m3)
Bleed stream

## Slide 28
28
Schematic process flow sheet for wet scrubber
Gypsum conditioning
Gypsum dosage
Flocculant
Reagents conditioning
Scrubber
Lime- stone & Dust
H2O
air
Kiln gas
H2O
old / new stack
H2O
H2O

## Slide 29
29
Quenching of raw gas at scrubber inlet to 55°C in order to protect lining of scrubber (PP)
High density of absorber sump that could damage scrubber components (controlled by bleed stream)
Bleed stream is mandatory in order to eliminate inerts (SiO2, etc) that would affect negatively the gypsum quality (size and hence dewatering)
pH of sump has to be kept at around 5
Gypsum conditioning
Key Issues – Critical points to be controlled

## Slide 30
30
Mandatory bleed stream in wet scrubbers
Centrifuge
Gypsum
Wet
Scrubber
Flocculant
Water
Waste water Bleed stream
Hydro- cyclone
Settling Tank
Bleed stream in order to eliminate inerts (SiO2, etc) that would affect negatively the gypsum quality

## Slide 31
31
Efficiency of different secondary measures
CAPEX (Mio USD)
0
5
10
15
20
25
30

## Slide 32
32
SO2 emissions depend on
  Type of kiln system SO2 emissions of preheater kilns are basically fuel independent – exception: SO2 from bypass (and unfavorable conditions in tower)
  Sulphur input by raw materials (high volatiles) / fuel (long kiln)
  Kiln operating conditions (volatility, bypass)
  Secondary reduction measures
Actual and future SO2 limits  secondary reduction necessary in many cases
Available technology allows SO2 reduction up to...
  ...60 % by dry hydrated lime addition
  ...75 % by semi-wet scrubbing systems
  ...98 % by wet scrubbers
Summary

## Slide 33
33
Questions/Remarks?