## Slide 1: Chemistry impact on Raw Material Extraction
Technical Development Program for PPE, 2015-2016

## Slide 2: MMT – RMPH Areas of Activities
Reserves, Mining, Preparation & Handling
Geological Investigation

## Slide 3: Process Overview
Material chemical homogeneity
Material size reduction
Material moisture reduction
Material handling

## Slide 4: Size Reduction
Blasting
Crushing
Grinding
Dosing for optimal size reduction process

## Slide 5: Moisture Reduction
Selective mining
Material dewatering / precipitation protection
Drying

## Slide 6: Sensitivity Analysis
The quarry is supposed to deliver raw materials according to the production needs of the plants
  These needs are typically defined in terms of LS, SR, AR, minor constituents like MgO, SO3, TOC etc.
The QSO “Optimizer” tool calculates the maximum achievable raw mix tonnage from a deposit, based on these requirements
The QSO “Batch Optimizer” does the same thing, but it allows to vary one (or two) of the parameters
  With this it can be seen which of the quality parameters are more or less critical in terms of possible changes due to production changes, product changes, corrective or AFR changes etc., and in which way they are critical

## Slide 7: Clear trend: SR Ibity
This example shows a clear trend: the higher the target SR, the higher the tonnage and the lower the waste ratio
Red line: currently defined target quality

## Slide 8: Tonnage maximum: MgO Ibity
Total achievable tonnage and lowest waste ratio from the Ibity quarry is highest with an average MgO around 2.3-2.4%
In order to realize such a MgO target, blasthole sampling and the use of QuarryMaster is required

## Slide 9: LS sensitivity
Minor sensitivity effect: LS Ibity
Very important sensitivity: LS Maratha

## Slide 10: For every change in raw material quality requirements consider the consequences for the quarry Message

## Slide 11: Message – Consequences of Quality Changes for the Quarry
Any major change in raw material quality requirements needs to be cross-checked with the Raw Material Management tools, to see the consequences for quarry lifetime, wasting etc.
  Having a sensitivity analysis allows to estimate already in advance
An indirect consequence is the need for recalculating long/medium term schedule quarry schedules
  And this in turn may require also an update for the mines planning and equipment optimization
Only based on this, the daily quarry operation can continue to work according to a long term view
  Short notice quality changes that are ordered from the quarry require a switch to “ad hoc” operation, ignoring any planning
  Such a “strategy” will most likely spoil the quarries long term potential

## Slide 12: Operation of Preblending Systems
Technical Development Program for PPE, 2015-2016

## Slide 13
13
Homogenisation Overview
Quarry operation
Crushing
Preblending
Mix proportioning
Raw mill
Homogenising
Kiln dust management
Short term
Long term

## Slide 14
14
Raw meal uniformity (sLSF after raw mill)
  Target short term (hourly samples over 24h): < 3.6
  Target long term (daily values over 1 month): < 1.0
Storage capacity sufficient for weekend operation
Parameters that influence blending efficiency
  Pile formation
    Chevron / chevcon / windrow stacking
    Front reclaiming
  Number of layers > 250
  Pile geometry
    LPS: Length / width ratio: > 4:1
    CPS: Stacking angle: 110-120°
Preblending System Design

## Slide 15
15
  Always complete piles
  Increasing stacker speed gives more layers (up to max. 35 m/min, consider the mechanical condition of the stacker
  Crusher capacity and preblending bed size have to match
e Blending efficiency
n Number of layers
A Pile cross-section
v Stacker travelling speed
q Stacking capacity
Blending Efficiency
with
(for statistically independent layers)

## Slide 16
16
The End Cone Effect
Operation of Preblending Systems

## Slide 17
17
Problem
  Peak disturbance when cutting a new pile
  Correcting by means of additive proportioning is possible but expensive symptom fighting
Solution
  Improved layering solves the problem at its source
Impact on Performance

## Slide 18
18
Layering pattern
  In the beginning only very few layers are reclaimed at a time
Segregation
  Coarse particles (often having a different chemical composition) tend to roll down the pile
  These particles are reclaimed first
Problem: End Cone Effect

## Slide 19
19
Instead of stacking all layers up to a single reversing point, make reversing points dependant of the stacking height. This
  reduces segregation
  allows to reclaim all layers from the beginning
Solution: Variable Stacker Reversing Points
Inner pile end
Outer pile end
reclaiming

## Slide 20
20
S
S
A
A
A
S
Sensor
Actuator
Sensors and encoders
  To determine angles, travel distances, speeds and stacker positions
Actuators
  For stacker operation
Requirements

## Slide 21
21
A number of reference points need to be fixed to the rails
  Marks for pile boundaries (as safety switches)
  Marks for the centre position between both piles
  Reference distance to correct encoder results for wheel slippage
Reference Points

## Slide 22
22
Pile Geometry

## Slide 23
23
Homogenising silo
  Reduced disturbances going into the silo
  Which can be handled better by the silo
Preblending system
  Reduced compositional peak disturbances when starting to reclaim from a new pile
Uniformity Improvement
t
t
LSF
LSF
fixed reversing points
variable reversing points

## Slide 24
24
Operation of Preblending Systems
Addition of Minor Components

## Slide 25
25
Raw mix adjustment by addition of minor components can be done in two ways
Raw Mix Adjustment
  By addition to the preblending system at the crusher
  Via feed bins to the raw mill feed

## Slide 26
26
The following concepts are not recommended
  Truck wise addition to the crusher  Leading to a patchwork distribution of the minor component
  Single layer addition to the crusher  Distribution depends on stacker position and is not consistent
Addition of Minor Components – Problematic Concepts
L
L

## Slide 27
27
Patchwork type addition of minor components
Addition of Minor Components – Problematic Concepts

## Slide 28
28
The following concepts are recommended
  Double layer addition to the crusher (forth and back movement of the stacker)  Only for longitudinal preblending systems
  Addition at controlled rate to the crusher via additional feed hopper
Addition of Minor Components – Recommended Concepts
J
J
J
J

## Slide 29
29
  Addition to the raw mill by means of a bin & feeder
    Selection of small feed bins
    Do not abuse feed bins as storage
    Do not control feed rates directly out of large storage silos
    Never feed several mills out of a common feed bin
    Always design feed bins for mass flow (according to material characteristics)
    Calibrate feeders regularly and keep them clean
Addition of Minor Components – Recommended Concepts

## Slide 30
30
Operation of Preblending Systems
Material Activation

## Slide 31
31
Improved material activation
  Use bows instead of pins on the rake
  Always adapt rake inclination to angle of repose
Insufficient material activation
  Difficult to handle material will not roll down the pile face
  Formation of deep channels
  Material is finally activated by rake structure  wear
Pile Face Activation

## Slide 32
32
Operation of Preblending Systems
Chain Life

## Slide 33
33
Design of the transition to the delivery chute
  Prefer a guided rail design over a sprocket wheel to prevent polygon effect
Impacts on Chain Life

## Slide 34
34
The traction function of the chain should be independent of guidance function in order to lower wear on rollers & guides
  Install rollers directly on the scraper supports rather than on the chain
Impacts on Chain Life

## Slide 35
35
Tension on both chain strands should be even
Do not over lubricate chains (to prevent material build-ups)
Reduce uneven wear on scrapers
Prevent material from falling on wheels (install covers)
Impacts on Chain Life

## Slide 36
36
Operation of Preblending Systems
Floor Grading

## Slide 37
37
Prevent floor compaction in order to
  Prevent reclaimer chain damage when switching pile
  Reduce power consumption and wear of scrapers
Install loosening teeth on scrapers
  Staggered pattern
Grade the floor once a year
Run the chain also when shunting
Floor Grading