## Slide 1: Raw Meal Homogenisation
Technical Development Program for PPE, 2015-2016

## Slide 2
2
Auditing of Blending Silos
Targets
Inspection
Sampling campaign
Common problems & solutions
Kiln dust handling
Contents

## Slide 3: Benefits of good homogeneity / uniformity
Reduced consumption of correctives
Lower kiln heat consumption
Lower refractory consumption
Possibility to increase TSR
Improved clinker reactivity
Improved clinker grindability
Lower electrical energy consumption
Lower cost!
Notes: SG: reduction STDEV from 2.5 to 1 , resulted in a reduction of the LS fet point by 2 points = 0.12 EUR/tck less in thermal cost (1’000 ktck/a)
TN: reduction of STDEV ? Led to a reduction of the heat consumption by 170 kJ/kgck = 225 kEUR/a (500 ktck/a)
SH: reduction STDEV from 3.01 to 2.1 in kiln feed = reduction heat consumption from 3.57 GJ/tck to 3.42 GJ/tck and improved clinker reactivity from 33 MPa to 35 MPa.
General FLS formula: -1% in lSF STDEV = - 100 kJ/kgck

## Slide 4
4
Targets
Raw Meal Homogenisation

## Slide 5
5
Auditing of Blending Silos
Check if targets are reached
  If they are not reached, find the root cause (quarrying, preblending, homogenising, …). If short term fluctuations are an issue
Test blending efficiency of homogenising silo
  If blending efficiency is lower than required (and lower than achievable with your silo system)
Check homogenising silo operation parameters

## Slide 6
6
Targets for Homogenising Silos
Raw meal: sLS < 3.6 (short term)
Kiln feed: sLS < 1.2 (short term)
Blending factor (BF) guide values:
> 5:1 for batch type mixing silos
< 5:1 for continuous blending silos (typically 3:1)
 BF depending on raw meal uniformity!

## Slide 7
7
Product Uniformity Targets
Short term
Hourly samples
over 24 h
Long term
Daily values over
one month
LS
s
< 1.2
< 1.0
SR
s
< 0.04
< 0.03
AR
s
< 0.04
< 0.03
Raw meal
< 3.6
< 1.0
Kiln feed
(or clinker)
ex mill
LS
s

## Slide 8
8
Three types of homogenising silos
  Batch type mixing silo
  Continuous blending silo
  Multi-pack silo
Refreshing the Basics
Storage silo
Homogenising silo
Most frequent old plants
Most frequent newer plants
Marginal spread

## Slide 9
9
Inspection
Raw Meal Homogenisation

## Slide 10
10
Drawings
Silo dimensions and volumes
Aeration system
  Number of aeration sectors and their arrangement
  Air pad dimensions and arrangement
  Blower specifications (air flow rates & pressures)
  Air distribution and type of valves
Checklist – System design - built

## Slide 11
11
Condition (tightness) of silo roof and walls
Raw meal coating on silo walls and bottom
Lump formation issues
Silo emptying degree
Raw mill distribution at silo feed (material layering)
Raw mill / kiln feed production rate
History of filling degree (operating range)
Sector aeration sequence and times
Kiln feed mode
Dust handling mode during direct kiln operation
Checklist – Equipment state – operation

## Slide 12
12
Checklist - Material Quality

## Slide 13
13
Sampling Campaign
Raw Meal Homogenisation

## Slide 14
14
Sampling
Define locations / set sampling ports
Spot samples, 1kg, every 30 mint, during 24 h at silo inlet & outlet (for batch silos: sample three batches).
Minimum 30 samples
Double sampling (two consecutive spot samples) in case of guarantee discussions
Parameters to be measured:
  Moduli (LSF, AR, SR)
  Moisture
  Fineness

## Slide 15
Evaluation
Aver. Input = 98.2
STDEV in = 5.5
Aver. Input = 99.2
STDEV out = 1.3
Remove outlayers = Aver I ± ~3 x STDEV
Blending factor =
STDEV in = 5.5
STDEV out = 1.3

## Slide 16
16
Common Problems & Solutions
Raw Meal Homogenisation

## Slide 17
17
Water ingress
  Seal roof and walls
Silo rains (condensation on silo roof)
  Investigate on insulation for silo roof
  Operate silo dedusting 24h
Wall condensation through wind chill
  Investigate on installation for wind shields and/or insulation
High residual moisture in raw meal
  Investigate on drying process before and in the raw mill
Lump Formation & Build-ups

## Slide 18
18
Segregation due to non uniform raw meal distribution
  No distribution spider on unfavourable design
  Inconsistent feed rate
  Unlevelled distribution box
  Eccentric feed point
Segregation in Silo

## Slide 19
19
Silo cleaning and air pad maintenance must be performed on a regular basis
When the silo is empty, only a small amount of material should remain between the air pads on the silo floor
Possible reasons for fabric blockages include
  Moist or contaminated aeration air (e.g. with oil)
  Broken fabric
Aeration Blockages

## Slide 20
20
Consider coating concrete structure and cone with special paint
  Abrade all surfaces using 40 grit sanding poles
  Vacuum clean to remove all dirt / dust
  Apply two coats of special paint at a normal 100μm dry film thickness
    E.g. “Dulux Durebild HSE” epoxy
Material Coating

## Slide 21
21
Too short aeration times (e.g. < 5min.)
  No proper material funnel can form
  Lower blending efficiency
  Material starvation close to the wall
Too long aeration times (e.g > 10min.)
  Shortcuts for fresh material  Low retention time
  Lower blending efficiency
Excessive Aeration Times
Short vs. long aeration

## Slide 22
22
Silo operation at low filling degrees
  Low number of material layers combined
  Operate continuous blending silos above 70% filling degree
Activate single sectors at a time rather than two opposite sectors
Do not aerate sectors sequentially, jump instead
  Prevents intersection of material funnels at surface
  Can have impact on structural forces
Inadequate Aeration Sequence

## Slide 23
23
Too little aeration air can lead to material starvation along the wall
Too much aeration can lead to non uniform extraction
  Manual distribution valves on silo wall should be completely open to activate this material, valves close to extraction are more closed
  Outer ring sectors need to be activated together with central chamber sectors
Amount of Aeration Air & Distribution
10%
100%
100%
100%

## Slide 24
24
Improve water / oil separation from air
Secure adequate permeability of air pads
  Replace fabrics when plugged
  When replacing air pad system, upgrade from ceramic tiles to fabric type
Check for leaks in the distribution system (soap test)
Secure proper functioning of air distribution valves (solenoid instead mechanical valve system)
Insufficient Aeration Air Quality

## Slide 25
25
Kiln Dust Management
Raw Meal Homogenisation

## Slide 26
26
There are several ways to handle kiln dust in
  Compound operation: Raw mill is operating
  Direct operation: Raw mill is stopped
The choice depends on
  Installation / arrangement
  Segregation factor (SF)
Kiln Dust Management

## Slide 27
27
Segregation factor
  Describes tendency to cause segregation problems
  Is an indication for high deviation of kiln dust chemistry from raw meal chemistry
Segregation Factor
Critical
Critical
Sf < 0.8
0.8 < Sf < 1.2
Sf > 1.2
or

## Slide 28
28
Compound operation: Raw meal and kiln dust to blending silo
Direct operation: Kiln dust to kiln feed bin
Option 1
SF not critical
(0.8 < SF < 1.2)
Standard arrangement
Step variations between compound and direct operation
  May become excessive with critical SF
Notes: A 4800 tpd kiln = 200 tph clinker = 320 t/h meal feed & 16 t/h – 32 t/h dust depending on top cyclone efficiency recovery
For
This allow a simple simulation based on

## Slide 29
29
Kiln dust always bypassing blending silo
Compound operation
Direct operation
Option 2
SF not critical
(0.8 < SF < 1.2)
Separate filter dust transport
Similar chemical composition of kiln dust during compound and direct operation
For critical SF to be evaluated

## Slide 30
30
Compound operation: Raw meal and kiln dust to blending silo
Direct operation: Kiln dust to separate dust bin
Option 3
SF critical
(0.8 > SF > 1.2)
Standard for critical SF
Expensive
Optional bypass for heavy metals and chlorine

## Slide 31
31
Annexes
Raw Meal Homogenisation

## Slide 32
32
Outlier test (according to GRUBB’s)
  Get rid of the results which are outside expectation (confidence interval) due to sampling and analysis errors
  G: Critical value (function of number of samples)
  S: Standard deviation
  X: Value
  X: Average of all values
  n: Number of samples
   Values higher than about 3 times the standard deviation are considered outliers
Evaluation (1/3)
n | G
20 | 2.884
25 | 3.009
30 | 3.103
40 | 3.240
60 | 3.411

## Slide 33
33
The blending factor
  Defined as the ratio of the incoming and outgoing product variability expressed as standard deviations (corrected by the sampling error)
Evaluation (2/3)

## Slide 34
34
Sampling and analysis errors
  Double sampling (two individual samples taken immediately after each other) allow for a calculation of the sampling / analytical error
  di: Difference between the double sample (x1a – x1b)
  serr: Standard deviation of sampling error
Evaluation (3/3)

## Slide 35
35
Spreadsheet available for blending efficiency evaluation
Spreadsheet for silo efficiency evaluation