## Slide 1: Common Problems and Solutions Bagfilter problems
General Description of Plant Problem/Situation

## Slide 2
2
General Plant Information
Kiln system: 4 SP
Clinker production: 2070 t/d
Heat consumption: 3400 kJ/kg
Plant elevation 450 m (i.e. ambient pressure = 960 mbar)
Gas volumes in front of filter:
  Compound operation (60%): 225‘000 Nm3/h wet @ 10%O2*
        18% moisture, T=95°C,
        pstat= -5 mbar
  Direct operation (40%): 185‘000 Nm3/h wet @ 7%O2*
        22% moisture, T=145°C,
        pstat = -10 mbar
    * O2 value refers to the measured value at that filter inlet
Equipment & Operational Data

## Slide 3
3
General Plant Information
Bagfilter system:
  High pressure pulse jet system (6 bar)
  6 compartments
  1512 Nomex bags used (PA), length 4 m
  Dimensions of filter:
    Length: 11.64 m
    Width: 8.6 m
    Height: 10.0 m
    Bag diam.: 160 mm
Equipment & Operational Data
3.04 m
3.04 m
2.52 m
3.88 m
3.88 m
3.88 m
In
Out
1.5 m
8.5 m

## Slide 4
4
General Plant Information
Bags per row: 14
Distance bags to wall: 75mm
Distance between bags in a row: 50mm
Distance between two rows: 50mm
Equipment & Operational Data
75 mm
75 mm
50 mm
50 mm
18 rows
18 rows
18 rows
18 rows*
18 rows
18 rows*
* In these compartments the cleaning system of 1 row is not working

## Slide 5
5
Problem
High Dp over cloth (>20mbar) (despite cleaning)
Dust emissions > 50 mg/Nm3
Traces of corrosion are visible in the clean gas plenum
Short lifetime of bags (<12 months)
General Description of Plant Problem
Filter under positive pressure as filter fan can not handle high Dp
Damaged bags

## Slide 6
6
Define Problem
Analyze Causes
  Propose Measurements and Checks to perform
  Identify most likely Causes
Identify Solutions
  Propose Solutions (List)
Problem Analysis and Discussion