## Slide 1
1
Kiln 1 & 2
Coating formation mainly in the cyclone cones of stage 3 and 4
Clogging of meal outlet of stage 3 and 4
More than 70% of all cyclone blockages occurred in stage 4
High pressure loss over riser (10 mbar)
Heavy build-up formation in the riser duct and kiln inlet
Info Card - Build-Up Location and Pressure Loss
3
4
4

## Slide 2
2
Small meal outlet of the cyclones (meal ducts), mainly in stages 3 and 4
In the preheater tower, some of the meal flaps were fixed in open position with a metallic wire to prevent that blocks of coating would get stuck there.
Small kiln inlet chamber. Velocities of up to 30 m/s at critical kiln inlet cross section.
Inadequate design of top stage cyclones dust loss of 26.6 t/h (13,7% on kiln feed)
Info Card - Design

## Slide 3
3
The kiln is operated at 2.1 rpm (3.0 rpm installed). The clinker microscopy shows, that the clinker has a too high retention time in the high temperature zone of the kiln (large alite crystal size).
Info Card - Kiln Speed

## Slide 4
4
Low clinker free lime values indicate a hard burning:
  CaOfree: 0.6%
Info Card - Free Lime

## Slide 5
5
TSR = 9%
High liquid AF feed rate fluctuations as well as fluctuations of the calorific value lead to an unstable kiln operation
Info Card - AFR

## Slide 6
6
The kiln inlet seal does not seal properly
False air intake at splash box of riser duct, false air at poke holes, inspection doors (often not closed).
Info Card - False Air I

## Slide 7
7
Info Card - False Air II

## Slide 8
8
Info Card - Alkali/Chlorine/Sulfur Balance
 | SO3 | K2O | Na2O | Cl
Total input (%cli) | 0.99 | 0.60 | 0.33 | 0.027
Total output (%cli) | 1.05 | 0.62 | 0.31 | 0.023
Hot meal (%) | 4.3 | 2.8 | 0.37 | 1.4
  Sulfur volatility: 0.81
  A/S ratio in clinker: 0.88
LOI: 24%

## Slide 9
9
Info Card - Hot Meal
Kiln 1
Hot Meal Evaluation
Hot Meal Evaluation
no encrustations
zone of increasing
encrustation
problems
0.0
0.2
0.4
0.6
0.8
1.0
1.2
1.4
1.6
1.8
2.0
2.2
2.4
2.6
2.8
3.0
0.0
0.5
1.0
1.5
2.0
2.5
3.0
3.5
4.0
4.5
5.0
5.5
6.0
% SO3
% Cl
frequent
blockages