## Slide 1: Alkali-Sulfur-Chlorine Balance Introduction
Technical Development Program SPREAD 2016

## Slide 2: Objectives and Scope
Objectives
  Consistency check of mass flows- and laboratory data (e.g. mass balance and chemical analysis)
  Assessment of coating and blockage problems
  Assessment of fuel mix (e.g. additional petcoke or AFR potential, short- and long-term fuel mix planning)
Scope
  Overall mass balance and individual balances for alkali (K2O, Na2O), sulfur and chlorine
  Assessment of alkali, sulfur and chlorine inputs
  Assessment of molar (Alk-Cl)/S-ratio
  Assessment of hot meal (e.g. sulfur volatilization)
  Balance can be extended to other critical elements if required (e.g. P2O5)

## Slide 3: Basic principle
Under stable conditions :
Massinput = Massoutput
Alkinput = Alkoutput
SO3 input = SO3 output
Clinput = Cloutput

## Slide 4: Preconditions and balance duration
The condition of the kiln needs to be stable
  No kiln stop, fuel mix or raw mix changes in the last 24 hours
  Stable build-up and coating situation
  Typical clinker free lime (no cold kiln)
The duration of the balance depends on the objectives
  Minimum 8 hours (better 24 hours) with hourly sampling to investigate temporary coating and blockage problems
  With weekly, monthly or yearly averages for short-, medium or long-term planning of fuel mix

## Slide 5: Balance boundary?
Raw Materials
Fuels
Clinker
Discarded Dust
Emissions

## Slide 6: A: Kiln System & Raw Material Preparation
Balance Boundary
Emissions: SO2, HCl
Fuels
Clinker
Raw Materials (pure; before mill !)
Dust discarded (e.g. added to cement)

## Slide 7: B: Kiln System
Clinker as measured
Bypass dust (LEPOL grate dust): removed from system (e.g. to cement)
Emissions: SO2, HCl
Kiln feed as fed (!): = raw meal (on dry) + recycled filter dust
Balance Boundary
Other input: = fuels + dust injection

## Slide 8: Balance boundary comparison
Boundary A
  The concentrations of alkalis, sulfur and chlorine coming from the raw materials are not influenced by the dust from the kiln
  Representative sampling and sample preparation of each raw material (before the mill; un-ground!) is difficult (except in case of wet preparation)
  Internal storage effects are not considered
Boundary B
  Representative sampling and sample preparation of the kiln feed and filter dust is comparatively simple
  The concentrations of alkalis, sulfur and chlorine in the kiln feed are influenced by the dust from the kiln (during raw meal grinding, dust recirculation)

## Slide 9: Material sampling
Boundary A
  Individual raw material components (e.g. blast hole samples)
  Fuels
  Clinker
  Filter dust (during direct operation for dry kilns)
  Bypass dust
  Hot meal (bottom cyclone stage)
Boundary B
  Kiln feed (incl. recirculated filter dust for dry kilns)
  Fuels
  Clinker
  Filter dust
  Bypass dust
  Hot meal (bottom cyclone stage)

## Slide 10: Material analysis
Kiln feed, clinker, filter dust, bypass dust, hot meal
  SO3, Na2O, K2O, (Cl) by XRF
  Cl by titration!
  LOI by loss in weight in furnace
  H2O by loss in weight in furnace
Fuels
  S by sulfur analyzer (e.g. Leco)
  Na2O, K2O from ash analysis by XRF
  Cl by titration (extract from calorimeter bomb)
  H2O by loss in weight or Karl-Fischer for AFR
  Ash content by loss in weight in furnace
  CV by bomb calorimeter
  Ultimate analysis by H-C-N analyzer

## Slide 11: Additional data
Mass flows
  Filter dust and bypass dust from measurement
  Kiln feed and fuels from CCR
  Clinker by calculation
Process & emission data
  Emissions data (SO2, HCl) during direct operation
  Hourly kiln process data
  Minute data for O2/CO

## Slide 12: Evaluation of results
Compilation of MS Excel Tool “Alk-S-Cl balance.xls”
Tool & Guideline available

## Slide 13: Evaluation of results
Comparison of actual numbers with guide values
Results of balance:
Relevant chlorine input
Sulfur input
SO3/Alk-Ratio
Sulfur-volatility
“Hot meal graph”