## Slide 1: Alkali-Sulfur-Chlorine Balance TASK
Technical Development Program SPREAD 2016

## Slide 2: Alk-S-Cl balance - Tasks
1
Filter dust extraction
Chlorine input from coal
Evaluation of results
2
3
4
Chlorine input from raw materials

## Slide 3: Task 1: Filter dust extraction
During the kiln heat balance a filter dust mass flow of 14.3 t/h has been measured
During direct operation all the filter dust is extracted from the kiln system and used as mineral component in cement production
The data for the Alk-S-Cl balance are averages of 5 days (Mon 0:00 to Fri 24:00). During this period the actual operating time was
  Kiln: 120 hours
  Raw mill: 84 hours
Please enter the kiln dust mass flows correctly in the Alk-S-Cl balance!

## Slide 4: Task 2: Coal analysis
The laboratory reports the following results for the fine coal (coal/petcoke mix) analysis on “as fired basis”:
  Sulfur = 2.21%S
  NCV = 26’190 kJ/kg
  Ash = 15.0%
  Ash analysis: K2O = 0.93%, Na2O = 0.32%
Please enter the data correctly in correctly in the Alk-S-Cl balance!

## Slide 5: Task 3: Chlorine input
The following parameters have been calculated by the Alk-S-Cl balance tool:
  “Relevant” chlorine input = 354 gCl/cli
  “Calculated” chlorine in clinker = 242 gCl/cli
How much is the chlorine input from the raw materials?
Why is there a large difference between the actual and “calculated” chlorine content in clinker?

## Slide 6: Task 4: Evaluation of results
Further results are shown on the “Evaluation” page of the Alk-S-Cl balance tool:
  SO3/Alk-ratio in clinker
  sulfur volatility
  Hot meal graph
Please compare the results with the guidelines?
How do you judge the situation of this kiln regarding build-up and blockage formation?