## Slide 1: Alkali-Sulfur-Chlorine Balance
Tips & Tricks
Technical Development Program SPREAD 2016

## Slide 2: Alk-S-Cl balance Tips & Tricks
1
Material sampling & analysis
Entering data
Pyritic sulfur in raw materials
2
3
4
Sulfur input from raw material
Hot meal
5
Sulfur input
3
4
Chlorine input
Sulfur volatility
5

## Slide 3: Tips and Tricks – Material sampling & analysis
Sampling
  Take samples whenever possible from flowing material streams (e.g. transfer chutes, conveyor belts, air slides)
Analytical accuracy
  Make sure that XRF is calibrated for the different materials
  Double check XRF chlorine analysis by titration!
  Chorine analysis in clinker is never fully representative as chlorine is not continuously discharged from kiln
Required analytical precision:
  Kiln feed minimum two digits, better three digits (e.g. 0.002%)
  Fuels, filter dust, bypass dust, hot meal minimum one digit, better two digits (e.g. 0.20%)
Notes: 3
Klicken Sie, um die Formate des Vorlagentextes zu bearbeiten
  Zweite Ebene
    Dritte Ebene
      Vierte Ebene
        Fünfte Ebene

## Slide 4: Tips and Tricks – Entering data
Make sure that
  the basis of the analytical results is known
  mass flows and analytical data are entered on the same basis
Kiln feed, clinker, filter dust, bypass dust
  Enter mass flows on “dry” basis as chemical analysis and LOI are typically expressed on “dry” basis
Fuels
  Enter mass flows on “as fired” basis as analytical data are typically also expressed on “as fired” basis
  LOI = 100 - ash content
  Alkalis from ash analysis (Alk = AlkAsh * ash content)
Notes: 4
Klicken Sie, um die Formate des Vorlagentextes zu bearbeiten
  Zweite Ebene
    Dritte Ebene
      Vierte Ebene
        Fünfte Ebene

## Slide 5: Tips and Tricks – Cross-checks
Mass balance
  Compare calculated top cyclone efficiency with typical values
Inputs from raw materials
  Compare raw meal calculated from kiln feed and filter dust (raw meal = kiln feed – recirculated filter dust)
  with raw meal calculated from raw materials (raw meal = S (% element in raw material * % in raw mix)
  and raw meal analysis (after raw mill)
Chlorine input
  Compare “relevant” chlorine input with chlorine in hot meal (rule of thumb: chlorine hot meal = 50 * relevant chlorine input)
Notes: 5
Klicken Sie, um die Formate des Vorlagentextes zu bearbeiten
  Zweite Ebene
    Dritte Ebene
      Vierte Ebene
        Fünfte Ebene

## Slide 6: Tips and Tricks – Pyritic sulfur in raw materials
Without wet scrubber
  already considered in filter dust and SO2 emissions
With wet scrubber
  sulfur captured in wet scrubber needs to be added as output
Notes: 6
Klicken Sie, um die Formate des Vorlagentextes zu bearbeiten
  Zweite Ebene
    Dritte Ebene
      Vierte Ebene
        Fünfte Ebene

## Slide 7: Tips and Tricks – Hot meal
In-line calciner (ILC) with two (or more) strings
  Take hot meal samples from both bottom cyclones
  Calculate weighted average based on split of kiln feed to different strings
Separate-line calciner (SLC)
  Take hot meal sample from calciner string for calciner control (LOI  calcination degree)
  Take hot meal sample from kiln string for hot meal assessment (hot meal graph) and calculation of sulfur volatility
Notes: 7
Klicken Sie, um die Formate des Vorlagentextes zu bearbeiten
  Zweite Ebene
    Dritte Ebene
      Vierte Ebene
        Fünfte Ebene

## Slide 8: Tips and Tricks – Chlorine input
If extracted dust must be mixed into cement, respect Cl limit of cement:
- typical chlorine limit cement: 0.1% Cl  upper limit for input:  800 g Cl/ t clinker - for higher chlorine inputs leaching of bypass dust to be considered

## Slide 9: Tips and Tricks – Sulfur input
Historical approach for maximum total sulfur input:
Depending on kiln system and specific conditions more total sulfur input is possible, benchmarks are:
Kiln System | Min. A/S [-] | Max. A/S [-] | Max. S input [%SO3 in cli]
WL - Long Wet Kilns | 0.8 | 1.2 | 1.0
DG - Grate Preheater Kilns |  |  | 
DL - Long Dry Kilns |  |  | 1.2
SP - Suspension Preheater Kilns | 0.5 |  | 1.7
PC - Precalciner Kilns | 0.4 |  | 2.0
  Total Sulfur input < 1.5 %SO3 in clinker 0.8 < Molar A/S-ratio < 1.2

## Slide 10: Tips and Tricks – Sulfur volatility
Sulfur volatility :
SO3 = %SO3 on clinker basis (LOIfree)
 < 0.7  ok
> 0.7  combustion problem
 > 0.9  serious combustion problem