## Slide 1: Heat and Mass balance
Tips and Tricks!
Technical Development Program
SPREAD 2016

## Slide 2: Critical points during measurements
Kiln dust loss
Clinker weigh out
Clinker temperature
Cooler waste air temperature
Temperature measurements
Gas analysis
Radiation measurement

## Slide 3: Mass flow measurements
Kiln dust loss
Done before/ after the heat balance
Raw mill is shut down for > 1 h before measurement is started
At least 1 full truck is weighted and required time is recorded
Conditioning tower dust needs to be measured too, if it is not included in filter dust already
Clinker rate
Weigh out is typically done with trucks and weight bridge
For at least 12h
Do not overfill trucks (clinker loss during transport to weight bridge)

## Slide 4: Clinker temperature
Insulated box method
Coating included but no direct contact with thermocouple

## Slide 5: Clinker temperature box
Insulated box
(Measuring box according to VDZ guidelines)

## Slide 6: Clinker temperature box
Thermocouple (tip in center of sample)

## Slide 7: Enough samples are required..
Exclude outliers!

## Slide 8: Temperature of cooler waste air
Measure temperature close to the cooler
Do cross check with temperature at the heat exchanger inlet (radiation of crushed clinker on roller crusher)
Consider peaks in measurement for averaging (e.g. use datalogger with different temperature probes connected)
Average gas temperatures of the entire cross section (similar to Prandtl measurement) and compare to fix installed temperature measurement
Avoid extracting cooler middle air during heat balance

## Slide 9: Temperature measurements
Temperature of fuel and transport air
  Measure surface temperature of fuel transport duct close to main or calciner burner with contact thermometer
Temperature of tertiary air
  Measure close to the cooler (temperature drop due to radiation and convection losses of tertiary air duct)
  Do not measure in kiln hood (radiation from clinker)
Temperature of the kiln feed
  Measure before rotary valve
  If no port is available use contact thermometer

## Slide 10: Gas properties measurements
Gas properties at preheater outlet double cyclones:
  Measure gas composition and temperature of each cyclone
  Do cross check in downcomer
Calciner exit (measured after bottom stage cyclone)
  Water cooled, ceramic or special steel type probe
  Check representativity of your measurement
Kiln inlet
  Only water cooled or ceramic probes withstand temperature
  Check representativity of measurement

## Slide 11: Radiation and convection
Emissivity needs to be adjusted to surface!
Crosscheck temperature of pyrometer with temperature measured with contact thermometer on painted surfaces
Use outer enveloping cylinder area for radiation loss of satellite coolers
Enveloping cylinder of satellite coolers

## Slide 12: Emissivity of painted surfaces
Even with new painting influence observed

## Slide 13: Painting influence

## Slide 14: Influence of emissivity
ε = 0.9
ε = 0.7
ε = 0.5

## Slide 15: Influence of dirt

## Slide 16: Comparison of different emissivities and wind speeds
Kiln shell segment

## Slide 17: Typical Emissivity Factors (e)
Type of surface Temperature 
Rough oxidized steel 100°C 1.0
Rough oxidized steel 400°C 0.9
White lime paint (on steel) 400°C 0.8
Aluminum paint (weathered) 100°C 0.4 - 0.7
Aluminum paint (new) 100°C 0.2 - 0.4
Al jacket (rolled sheet material) 100 - 500°C 0.08
Al jacket (polished / bright foil) 100 - 500°C 0.04
 Set correct emissivity factor e on pyrometer if e is set too high, Pyrometer indicates too low if e is set too low, Pyrometer indicates too high
e.g. kiln shell, satellites
e.g. cyclone shell, calciner

## Slide 18: Procedure for evaluation of Heat / Mass balance
Compile all gas and mass flow measurements and convert them on a normalized, average hourly basis
Average all temperature measurements and gas analyses using PLC / TIS data and correct average where necessary by offset
Average data from lab
Fill in raw data in HBL spreadsheet
Tune heat balance in the following order:
  Mass balance
  Cooler air balance
  Cooler heat balance
  Kiln system heat balance

## Slide 19: Tuning mass balance
Clinker weight carried out:
Kiln feed/clinker factor reasonable?
Kiln heat consumption reasonable?
All dust losses reasonable and considered?
LOI of kiln feed and dust losses reasonable?
LOI of clinker set to 0 % (weighted clinker LOI free)?
If unsatisfactory error persists
  Recheck calibration of feeders and scales
  Repeat mass balance only
No clinker weight carried out:
Calculate clinker rate by setting mass balance error to zero
Kiln feed / clinker factor reasonable?
Kiln heat consumption reasonable?
Error < 1 %: good
Error < 3 %: satisfactory
Error > 3 %: unsatisfactory
If unsatisfactory, check:

## Slide 20: Mass balance guide values
 | Guide value | Comment
Kiln feed / clinker factor | 1.6 – 1.75 | Mostly dependent on PH (and bypass) dust loss High values of kiln feed LOI (> 35.5 – 36.0 %) only explicable if high LSF, high MgCO3 or burnable matter For high bypass dust rates, higher values possible
Cyclone efficiency | 90 – 95 % | Mainly a function of cyclone design, dip tube velocity, dip tube length, efficiency 2nd highest cyclone stage, kiln feed fineness (….)

## Slide 21: Tuning cooler air balance
Airflow measurement done:
Prandtl measurement point at waste air duct adequate and temperature representative
Measured cooler middle air flow reasonable?
Additional false air (e.g. AA-HE, filter, etc.) considered?
Cooler air flow vs. clinker end temperature reasonable?
False air (kiln hood, cooler, crusher) considered?
If unsatisfactory error persists
  Calculate waste air by zeroizing air balance error
No flow measurement:
Adjust waste air flow to set air balance error zero
Check the following points:
Cooler air flow versus clinker end temperature reasonable?
False air in kiln hood, cooler crusher considered?
Error < 1 %: good
Error < 3 %: satisfactory
Error > 3 %: unsatisfactory
If unsatisfactory, check:

## Slide 22: Cooler air balance
Typical correlation in-between cooler air flow and clinker end temperature for judgment of specific cooler air flow rate
Conventional grate cooler (old design)
Modern, high efficient cooler (new design)

## Slide 23: Cooler air balance guide values
 | Guide value | Comment
False air | Kiln inlet seal: 0.02 – 0.05 Nm3/kg cli Kiln hood: 0.01 – 0.03 Nm3/kg cli Cooler: 0.03 –0.05 Nm3/kg cli | Values refer to normal operating conditions (kiln hood pressure: - 0.5 to - 1.0 mbar kiln inlet pressure: - 2 to - 5 mbar) and a normal tight kiln system In case of lower (less negative) pressures, lower values acceptable In case of “big holes and gaps”, higher values acceptable Check clinker crusher for false air intake!!! Check tightness of pressurized double pendulum flaps / internal drag chain under grate (negative false air input!!)

## Slide 24: Tuning cooler heat balance
Check the following points:
Difference in-between secondary and tertiary air temperature reasonable? (<100 °C if common take off point)
Normalized cooler efficiency reasonable?
Clinker end temperature reasonable?
Radiation loss of satellite cooler reasonable (~250 – 350 kJ/kg cli)
If results are not reasonable:
Waste air temperature at border limit (close to cooler extraction) representative (average of entire cross section)??
Tertiary air temperature measurement representative?
False air (kiln hood, cooler, crusher) considered correctly??
Cooler air flow vs. clinker end temperature reasonable??
Secondary air typically not measured
Influence of radiation from hot clinker bed on measured temperature
Secondary air temperature used as fitting parameter to minimize cooler heat balance error
Error < 1 %: good
Error < 3 %: satisfactory
Error > 5 %: unsatisfactory
If unsatisfactory, check:

## Slide 25: Cooler heat balance guide values
 | Guide value | Comment
Normalized cooler efficiency (based on 0.8 Nm3/kg cli) | Modern grate cooler: 70 – 75 % Conventional grate cooler: 55 – 70 % Satellite cooler: 55 – 65 % (tube only) 60 – 70 % (incl. kiln internal cooling zone) | Efficiency of the cooler depends strongly on the condition (e.g. gap width in-between plates / seals) and design of the cooler (e.g. installation of fixed inlet), on the clinker granulometry (and porosity) as well as on operating conditions (no red rivers, geysers,….)

## Slide 26: Tuning kiln heat balance
Balance error:
Error < 1 %: excellent
Error < 3 %: good
Error > 5 %: unsatisfactory
Check the following points:
Kiln exhaust gas and cooler waste air losses reasonable?
Heat of clinker formation reasonable (default: 1750 kJ/kg)?
Burnable matter in kiln feed (TOC, pyrite) considered?
Radiation and convection losses reasonable?
Recheck calibration of fuel feeders and NCV determination
If unsatisfactory error persists:
Repeat heat balance

## Slide 27: Kiln heat balance guide values
 | Guide value | Comment
Specific heat consumption of kiln system | 4 stage PH or PC kiln: 3200 – 3500 kJ/kg cli 5 stage PH or PC kiln: 3100 – 3400 kJ/kg cli | Increased heat consumption due to AFR usage not considered