## Slide 1: Clinker Cooler Air Distribution Solution
Technical Development Program SPREAD 2016

## Slide 2: Air Distribution Clinker Cooler
Cooling air measurements have been made
Using the Cooler Assessment Tool, evaluate the data and assess the clinker cooler operation
  Use the “Guidelines and hints” tab
  What are your main findings?
  For each finding, what is the possible effect on operation?
  What are your recommendations?
  Assess the cooling air distribution. How can you improve?

## Slide 3: Cooler Aeration Scheme

## Slide 4: Cooler static inlet with horseshoe

## Slide 5: A Closer Look - Clinker Cooler Air Distribution
All measured data should be converted to ambient conditions at the fan inlet side

## Slide 6: Specific Task
The flow of fan 7 has been measured in the duct between the fan and cooler side wall: 31’339 Am3/h at 32°C
  Convert this air flow to ambient conditions at the fan inlet

## Slide 7: Solution
The flow of fan 7 has been measured in the duct between the fan and cooler side wall: 31’339 Am3/h at 32°C
  Convert this air flow to ambient conditions at the fan inlet

## Slide 8: Main Findings
Main findings
  Air flow profile: High flow behind static inlet  negative impact on heat recuperation
  Undergrate pressure profile: Flat pressure profile behind static inlet  unsealed compartments
  Specific cooler area load: 47.2 t/d/m2 (slightly on high side)
  Specific grate width load: 1’326 t/d/m (in normal range)
  Installed cooling air volume: 2.209 Nm3/kgcli (in normal range)
  Specific cooling air in operation: 1.984 Nm3/kgcli (in normal range)
  Clinker bed height: 450 mm on 1st grate Clinker bed height calculation matches with under grate pressure behind the static inlet (44 mbar)
  Clinker temperature drop on static inlet: 319°C  Split required (see next slide)
  Clinker temperature drop of compartment 2 too high due to too high air flow.  Reduce air flow when compartments are sealed!
  Calibration required for fans 1, 2 and 6
Expected operational problems
  High clinker temperature 160°C due to too low clinker bed
  Unsealed compartments: Air losses into cold clinker areas
  Reduced cooler efficiency

## Slide 9: Split static inlet